Supplementary Information

A new approach to very high lithium salt content quasi-solid state electrolytes for lithium metal batteries using plastic crystals

Danah Al-Masri,a Ruhamah Yunis,a Haijin Zhu,a Liyu Jin,b Peter Bruce,b Anthony F. Hollenkampc and Jennifer M. Pringlea

a Deakin University, Melbourne, Institute for Frontier Materials, Victoria 3125, Australia. Email:jenny.pringle@deakin.edu.au.

b Department of Materials Chemistry, University of Oxford, Parks Road, Oxford OX1 3PH, UK.

c Commonwealth Scientiﬁc and Industrial Research Organisation (CSIRO), Clayton, 3168, VIC, Australia.

Table S1. Transition temperatures (onset) and entropies for the [C2epyr][FSI]/Li[FSI] salts, Ts = solid–solid transition, Tm = melting. Data for Li[FSI] obtained from ref [1]

|  | Ts (°C ) ± 1 | ∆S (J K-1 mol-1) ± 10% | Tm(°C ) ± 1 | ∆S (J K-1 mol-1) ± 10% |
| --- | --- | --- | --- | --- |
| [C2epyr][FSI] | -35 | 36 | 129 | 9 |
| 90mol% LiFSI in [C2epyr][FSI] | -50 | 1 | 94 | 28 |
| Li[FSI] [1] | -51 | 2 | 140 | 41 |

Figure S1. 8 kHz MAS 19F NMR spectra of neat [C2epyr][FSI], neat Li [FSI] and 90 mol% Li[FSI] in [C2epyr][FSI].

Figure S2. Cyclic voltammogram of the quasi-solid state 90 mol% Li[FSI] in [C2epyr][FSI] electrolyte at 50°C. The arrows show the direction of peak progression from the 1st to the 4th scan, with platinum working electrode (2.0 mm2 surface area), lithium strip as a quasi-reference electrode and a coiled lithium metal strip as counter electrode.

Figure S3. The Nyquist plots obtained after select plating cycles in a Li | Li symmetrical cell containing the quasi-solid 90 mol% Li[FSI] in [C2epyr][FSI]. Cycling data shown in Figure 5 (a).

References.

[1]	Y. Zhou, X. Wang, H. Zhu, M. Yoshizawa‐Fujita, Y. Miyachi, M. Armand, M. Forsyth, G. W. Greene, J. M. Pringle, P. C. J. C. Howlett, ChemSusChem 2017, 10, 3135.