Supplementary Information

Shifting-reference concentration cells to refine composition-dependent transport characterization of binary lithium-ion electrolytes

Andrew A. Wang a, Tianhong Hou a, Minnie Karanjavala a, Charles W. Monroe a, b, *

a ﻿Department of Engineering Science, University of Oxford, Parks Road, Oxford, OX1 3PJ, United Kingdom.

b ﻿ ﻿The Faraday Institution, Harwell Campus, Didcot, OX11 0RA, United Kingdom.

* Corresponding Author – Email: charles.monroe@eng.ox.ac.uk

Table S1. Summary of density-composition calibration measurements for LiPF6:EMC solutions. Recorded under an argon atmosphere in a glovebox. Temperatures are accurate within 0.02 °C.

| mLiPF6 [g] | mEMC [g] | ω | ρ20°C [g/L] | ρ25°C [g/L] | ρ30°C [g/L] |
| --- | --- | --- | --- | --- | --- |
| 0.0000 | 10.0523 | 0.00000E+00 | 1013.1 | 1007.1 | 1001.1 |
| 0.0466 | 10.0145 | 4.63170E-03 | 1016.5 | 1010.5 | 1004.5 |
| 0.1502 | 10.0020 | 1.47948E-02 | 1023.2 | 1017.3 | 1011.2 |
| 0.4981 | 9.3821 | 5.04145E-02 | 1049.6 | 1043.7 | 1037.8 |
| 0.8075 | 9.9860 | 7.48135E-02 | 1068.5 | 1062.6 | 1056.7 |
| 1.0395 | 9.9670 | 9.44442E-02 | 1084.6 | 1078.8 | 1073.0 |
| 1.5037 | 9.9434 | 1.31361E-01 | 1114.7 | 1108.9 | 1103.1 |
| 1.9668 | 11.0127 | 1.51531E-01 | 1131.4 | 1125.7 | 1119.9 |
| 2.1150 | 10.0013 | 1.74558E-01 | 1150.6 | 1144.9 | 1139.2 |
| 2.5535 | 10.0793 | 2.02133E-01 | 1175.3 | 1169.6 | 1164.0 |
| 2.7691 | 10.0052 | 2.16771E-01 | 1189.1 | 1183.5 | 1177.9 |
| 3.0231 | 10.0040 | 2.32062E-01 | 1202.3 | 1196.8 | 1191.2 |
| 3.1650 | 10.2081 | 2.36669E-01 | 1205.3 | 1199.8 | 1194.2 |
| 3.3133 | 9.8747 | 2.51236E-01 | 1219.1 | 1213.6 | 1208.0 |
| 3.4413 | 9.6132 | 2.63610E-01 | 1230.8 | 1225.3 | 1219.8 |
| 4.2843 | 10.3339 | 2.93080E-01 | 1255.5 | 1250.0 | 1244.6 |

Table S2. Summary of Hittorf-cell measurements for LiPF6:EMC solutions. Transference numbers were calculated following section 2.4 in the main text.

| ρ20°Cinitial [g/L] | IpulseTpulse [C] | ρ20°Canodic [g/L] | ρ20°Ccathodic [g/L] | t+0 anodic | t+0 cathodic |
| --- | --- | --- | --- | --- | --- |
| 1033.7 | 14.1316 | 1036.1 | 1031.3 | 0.388 | 0.389 |
| 1033.7 | 14.2718 | 1036.1 | 1031.2 | 0.394 | 0.370 |
| 1033.8 | 14.4155 | 1036.2 | 1031.3 | 0.400 | 0.376 |
| 1065.7 | 17.03 | 1068.6 | 1062.7 | 0.358 | 0.338 |
| 1065.9 | 16.32 | 1068.8 | 1063.1 | 0.330 | 0.355 |
| 1067.4 | 14.1701 | 1069.9 | 1065.0 | 0.334 | 0.362 |
| 1067.6 | 14.3684 | 1070.1 | 1065.1 | 0.343 | 0.344 |
| 1119.2 | 14.4239 | 1121.7 | 1116.7 | 0.304 | 0.305 |
| 1119.1 | 14.389 | 1121.6 | 1116.7 | 0.303 | 0.332 |
| 1119.2 | 14.355 | 1121.6 | 1116.8 | 0.329 | 0.330 |
| 1170.6 | 14.4125 | 1173.1 | 1168.0 | 0.262 | 0.233 |
| 1170.8 | 14.2758 | 1173.3 | 1168.2 | 0.255 | 0.226 |
| 1171.8 | 14.3714 | 1174.4 | 1169.3 | 0.229 | 0.260 |
| 1220.4 | 14.4157 | 1222.8 | 1218.0 | 0.250 | 0.251 |
| 1220.3 | 14.412 | 1222.7 | 1217.9 | 0.250 | 0.251 |
| 1220.2 | 14.277 | 1222.6 | 1217.9 | 0.243 | 0.275 |
| 1268.3 | 14.3747 | 1270.5 | 1266.0 | 0.270 | 0.238 |
| 1268.3 | 14.3747 | 1270.6 | 1266.0 | 0.237 | 0.238 |
| 1268.2 | 14.4146 | 1270.4 | 1266.0 | 0.272 | 0.273 |
| 1268.3 | 14.4146 | 1270.6 | 1266.0 | 0.239 | 0.240 |

Table S3. Summary liquid-junction potentials in concentration cells for LiPF6:EMC at 25 °C. Data presented in figure 4 (a) is arrived at by interchanging ρ25 °CA and ρ25 °CB between reference and test concentrations to achieve a full matrix of results.

| ρ25 °CA [g/L] | ρ25 °CB [g/L] | U [mV] | SD [mV] |
| --- | --- | --- | --- |
| 1008.3 | 1012.6 | 19.73 | 0.40 |
| 1008.3 | 1017.6 | 25.47 | 1.37 |
| 1012.6 | 1017.6 | 6.46 | 0.40 |
| 1012.6 | 1027.8 | 12.24 | 0.70 |
| 1017.6 | 1027.8 | 4.03 | 0.08 |
| 1017.6 | 1048.7 | 15.65 | 0.22 |
| 1027.8 | 1048.7 | 6.73 | 0.24 |
| 1027.8 | 1072.2 | 10.37 | 0.15 |
| 1048.7 | 1072.2 | 4.01 | 0.32 |
| 1048.7 | 1093.9 | 8.30 | 0.08 |
| 1072.2 | 1093.9 | 4.70 | 0.35 |
| 1072.2 | 1114.8 | 10.06 | 0.40 |
| 1093.9 | 1114.8 | 5.89 | 0.58 |
| 1093.9 | 1136.3 | 11.98 | 0.47 |
| 1114.8 | 1136.3 | 6.11 | 0.85 |
| 1114.8 | 1155.6 | 14.43 | 0.26 |
| 1136.3 | 1155.6 | 7.32 | 0.11 |
| 1136.3 | 1165.9 | 12.65 | 0.33 |
| 1155.6 | 1165.9 | 4.14 | 0.28 |
| 1155.6 | 1193.0 | 21.27 | 0.30 |
| 1165.9 | 1193.0 | 15.99 | 0.27 |
| 1165.9 | 1209.0 | 24.41 | 2.53 |
| 1193.0 | 1209.0 | 11.61 | 1.01 |
| 1193.0 | 1229.5 | 30.87 | 0.31 |
| 1209.0 | 1229.5 | 18.99 | 0.23 |
| 1209.0 | 1246.3 | 37.62 | 0.21 |
| 1229.5 | 1246.3 | 15.48 | 0.44 |
| 1229.5 | 1268.1 | 35.33 | 1.31 |
| 1246.3 | 1268.1 | 20.50 | 0.26 |
| 1246.3 | 1285.4 | 41.12 | 0.92 |
| 1268.1 | 1285.4 | 20.75 | 0.16 |
| 1268.1 | 1299.8 | 37.79 | 0.13 |
| 1285.4 | 1299.8 | 16.87 | 0.63 |
| 1285.4 | 1317.0 | 38.41 | 0.26 |
| 1299.8 | 1317.0 | 21.52 | 0.07 |
| 1299.8 | 1333.6 | 43.61 | 0.20 |
| 1317.0 | 1333.6 | 22.12 | 0.68 |
| 1317.0 | 1361.4 | 61.83 | 0.43 |
| 1333.6 | 1361.4 | 39.82 | 0.16 |

Table S4. Summary liquid-junction potentials in concentration cells for LiPF6:PC at 25 °C. Data presented in figure 4 (b) is arrived at by interchanging ρ25 °CA and ρ25 °CB between reference and test concentrations to achieve a full matrix of results.

| ρ25 °CA [g/L] | ρ25 °CB [g/L] | U [mV] | SD [mV] |
| --- | --- | --- | --- |
| 1203.4 | 1203.8 | 19.44 | 0.51 |
| 1203.4 | 1204.6 | 55.30 | 1.46 |
| 1203.8 | 1204.6 | 20.89 | 0.55 |
| 1203.8 | 1205.6 | 44.40 | 1.17 |
| 1204.6 | 1205.6 | 13.93 | 0.55 |
| 1204.6 | 1207.1 | 32.76 | 0.87 |
| 1205.6 | 1207.1 | 15.22 | 0.40 |
| 1205.6 | 1208.7 | 38.49 | 1.02 |
| 1207.1 | 1208.7 | 9.19 | 0.24 |
| 1207.1 | 1210.7 | 21.99 | 0.58 |
| 1212.2 | 1219.9 | 23.50 | 0.62 |
| 1212.2 | 1227.4 | 44.78 | 0.80 |
| 1219.9 | 1227.4 | 17.35 | 0.26 |
| 1219.9 | 1234.7 | 28.26 | 1.17 |
| 1227.4 | 1234.7 | 12.74 | 0.40 |
| 1227.4 | 1243.2 | 22.17 | 0.25 |
| 1234.7 | 1243.2 | 10.99 | 0.26 |
| 1234.7 | 1251.3 | 17.92 | 0.08 |
| 1243.2 | 1251.3 | 11.04 | 0.14 |
| 1243.2 | 1260.0 | 17.12 | 0.04 |
| 1248.2 | 1257.3 | 9.61 | 0.35 |
| 1248.2 | 1270.5 | 19.36 | 0.61 |
| 1257.3 | 1264.6 | 8.67 | 0.01 |
| 1257.3 | 1273.6 | 17.38 | 0.09 |
| 1264.6 | 1273.6 | 9.48 | 0.20 |
| 1264.6 | 1283.8 | 19.38 | 0.14 |
| 1273.6 | 1283.8 | 11.79 | 0.52 |
| 1273.6 | 1291.0 | 18.40 | 0.09 |
| 1283.8 | 1291.0 | 7.31 | 0.24 |
| 1283.8 | 1298.6 | 14.57 | 1.00 |
| 1291.0 | 1298.6 | 8.35 | 0.64 |
| 1291.0 | 1306.6 | 17.20 | 0.24 |
| 1298.6 | 1306.6 | 8.39 | 0.42 |
| 1298.6 | 1314.3 | 16.67 | 0.72 |
| 1306.6 | 1314.3 | 8.17 | 0.41 |
| 1306.6 | 1322.2 | 16.30 | 0.14 |
| 1314.3 | 1322.2 | 8.75 | 0.21 |
| 1314.3 | 1329.9 | 14.01 | 0.18 |

Table S4. Continued

| ρ25 °CA [g/L] | ρ25 °CB [g/L] | U [mV] | SD [mV] |
| --- | --- | --- | --- |
| 1322.2 | 1329.9 | 7.30 | 0.11 |
| 1322.2 | 1338.2 | 16.36 | 0.27 |
| 1329.9 | 1338.2 | 9.71 | 0.30 |
| 1329.9 | 1346.9 | 18.28 | 0.32 |
| 1338.2 | 1346.9 | 8.76 | 0.06 |
| 1338.2 | 1353.5 | 20.13 | 0.30 |
| 1346.9 | 1353.5 | 8.91 | 0.15 |
| 1346.9 | 1361.9 | 19.55 | 0.47 |
| 1353.5 | 1361.9 | 8.23 | 0.38 |
| 1353.5 | 1368.9 | 18.14 | 0.13 |
| 1361.9 | 1368.9 | 9.69 | 0.23 |
| 1361.9 | 1376.7 | 17.14 | 0.08 |
| 1368.9 | 1376.7 | 7.74 | 0.08 |
| 1368.9 | 1382.7 | 15.01 | 0.11 |

Table S5. Summary of ionic conductivity measurements for LiPF6:EMC solutions.

| ρ20 °C [g/L] | κ20 °C [μS/cm] | κ25 °C [μS/cm] | κ30 °C [μS/cm] |
| --- | --- | --- | --- |
| 1018.9 | 0.349 | 0.503 | 0.668 |
| 1023.2 | 5.995 | 6.321 | 6.568 |
| 1034.6 | 117.3 | 119.8 | 121.0 |
| 1049.6 | 611.1 | 634.6 | 655.1 |
| 1068.5 | 1492 | 1563 | 1632 |
| 1084.6 | 2406 | 2533 | 2654 |
| 1114.7 | 4045 | 4294 | 4536 |
| 1131.4 | 4760 | 5100 | 5433 |
| 1175.3 | 5705 | 6212 | 6688 |
| 1205.3 | 5452 | 5996 | 6560 |
| 1230.8 | 4836 | 5401 | 5983 |

# Figure S1 measured ionic conductivities (x) of LiPF6:EMC at 20, 25, and 30 °C.

Fitting process for equivalent conductance

A power series in y1/4 was used to fit equivalent-conductance data. The general form studied with the optimization algorithm was

| Λ=Λ0+k=17Λkyk22. | (S1) |
| --- | --- |

By minimizing number of parameters, maximizing R2, and minimizing the root-mean-squared error (RMSE) in the 95% confidence interval, it was found that a 3-parameter fit with average R2 = 0.9997 and average confidence interval RMSE = 0.077 was optimal, using the programmatic Curve Fitting Toolbox by MathWorks, which returned best-fit parameter values as a vector Λk,CIleft,k,CIright,k, where CIleft,k and CIright,k respectively represent the lower and upper bounds of the 95% confidence interval (CI) on Λk.

For each possible collection of nonzero parameters in equation S1, CI RMSE was calculated with the formula

| RMSECI=1nterms≠0k:Λk≠0`CIright,k-CIleft,kΛk2. | (S2) |
| --- | --- |

We note that 0 always fell between the confidence intervals for the constant term Λ0, and so it was not included in the final correlation. The presence of Λ0 has physical meaning for strong electrolytes, which would be expected to obey Onsager–Fuoss conductance law at limiting dilution, but does not appear to be justified for LiPF6:EMC based on our experimental data.

This process identified the error-minimizing final functional form to be

|  | Λ = Λ1y1/2+Λ2y+Λ3y5/22, | (S3) |
| --- | --- | --- |

equation 19 in the main-body text.

Table S6. Summary of dynamic viscosity measurements for LiPF6:EMC solutions.

| ρ20 °C [g/L] | η20 °C [mPa•s] | η25 °C [mPa•s] | η30 °C [mPa•s] |
| --- | --- | --- | --- |
| 1013.1 | 0.724 | 0.680 | 0.639 |
| 1015.8 | 0.745 | 0.686 | 0.644 |
| 1025.6 | 0.778 | 0.743 | 0.701 |
| 1041.9 | 0.916 | 0.877 | 0.808 |
| 1064.5 | 1.143 | 1.063 | 1.000 |
| 1093.9 | 1.524 | 1.405 | 1.294 |
| 1119.6 | 1.994 | 1.825 | 1.673 |
| 1169.9 | 3.570 | 3.176 | 2.860 |
| 1215.6 | 6.726 | 5.807 | 5.104 |
| 1245.2 | 10.650 | 9.797 | 8.648 |

Table S7. Summary of dynamic viscosity measurements for LiPF6:PC solutions.

| ρ20 °C [g/L] | η20 °C [mPa•s] | η25 °C [mPa•s] | η30 °C [mPa•s] |
| --- | --- | --- | --- |
| 1204.9 | 2.74 | 2.47 | 2.24 |
| 1213.3 | 3.008 | 2.707 | 2.449 |
| 1216.0 | 3.362 | 3.038 | 2.734 |
| 1237.7 | 4.229 | 3.766 | 3.374 |
| 1253.6 | 5.394 | 4.75 | 4.218 |
| 1269.9 | 7.899 | 6.132 | 5.373 |
| 1285.8 | 9.461 | 8.129 | 7.04 |
| 1300.0 | 12.48 | 10.59 | 9.033 |
| 1316.8 | 17.89 | 14.83 | 12.36 |
| 1332.0 | 25.08 | 20.43 | 16.85 |
| 1361.0 | 55.72 | 42.93 | 34.02 |

Table S8. Summary of restricted-diffusion measurements for LiPF6:EMC solutions. κeff was obtained using electrochemical impedance spectroscopy (EIS)

| ρ20 °C [g/L] | slope fit [s-1] | Deff [cm2/s] | κeff [mS/cm] | b |
| --- | --- | --- | --- | --- |
| 1020.1 | 1.18E-03 | 4.77E-06 | 9.34E-04 | 0.58 |
| 1020.1 | 1.29E-03 | 5.22E-06 | 9.24E-04 | 0.65 |
| 1020.1 | 1.04E-03 | 4.21E-06 | 8.52E-04 | 1.15 |
| 1020.1 | 7.88E-04 | 3.19E-06 | 7.70E-04 | 1.77 |
| 1025.3 | 1.16E-03 | 4.69E-06 | 1.23E-02 | 0.32 |
| 1025.3 | 9.41E-04 | 3.81E-06 | 1.02E-02 | 1.45 |
| 1025.3 | 1.02E-03 | 4.13E-06 | 1.20E-02 | 0.45 |
| 1025.3 | 9.51E-04 | 3.85E-06 | 1.17E-02 | 0.58 |
| 1049.3 | 6.13E-04 | 2.49E-06 | 0.398 | 2.79 |
| 1049.3 | 7.09E-04 | 2.87E-06 | 0.490 | 1.51 |
| 1049.3 | 5.42E-04 | 2.20E-06 | 0.395 | 2.84 |
| 1049.3 | 8.41E-04 | 3.41E-06 | 0.521 | 1.14 |
| 1094.7 | 6.47E-04 | 2.62E-06 | 2.51 | 1.07 |
| 1094.7 | 5.29E-04 | 2.14E-06 | 2.03 | 2.36 |
| 1094.7 | 7.42E-04 | 3.01E-06 | 2.87 | 0.25 |
| 1094.7 | 5.42E-04 | 2.20E-06 | 2.09 | 2.20 |
| 1094.7 | 5.42E-04 | 2.19E-06 | 2.18 | 1.92 |
| 1117.9 | 6.55E-04 | 2.65E-06 | 3.58 | 1.03 |
| 1117.9 | 5.11E-04 | 2.07E-06 | 3.32 | 1.49 |
| 1117.9 | 5.49E-04 | 2.23E-06 | 3.80 | 0.66 |
| 1117.9 | 5.97E-04 | 2.42E-06 | 4.01 | 0.34 |
| 1117.9 | 5.31E-04 | 2.15E-06 | 3.38 | 1.39 |
| 1117.9 | 5.72E-04 | 2.32E-06 | 3.53 | 1.11 |
| 1178.8 | 4.47E-04 | 1.81E-06 | 4.52 | 1.46 |
| 1178.8 | 3.97E-04 | 1.61E-06 | 4.26 | 1.83 |
| 1178.8 | 5.43E-04 | 2.20E-06 | 5.09 | 0.73 |
| 1178.8 | 4.40E-04 | 1.78E-06 | 4.76 | 1.14 |
| 1215.3 | 4.32E-04 | 1.75E-06 | 4.12 | 1.38 |
| 1215.3 | 3.45E-04 | 1.40E-06 | 4.63 | 0.66 |
| 1215.3 | 5.18E-04 | 2.10E-06 | 5.01 | 0.18 |
| 1215.3 | 3.39E-04 | 1.37E-06 | 4.59 | 0.72 |
| 1215.3 | 2.62E-04 | 1.06E-06 | 4.74 | 0.52 |
| 1255.5 | 3.85E-04 | 1.56E-06 | 4.38 | 0.29 |
| 1255.5 | 2.46E-04 | 9.99E-07 | 3.66 | 1.38 |
| 1255.5 | 2.06E-04 | 8.35E-07 | 3.07 | 2.47 |
| 1255.5 | 2.07E-04 | 8.41E-07 | 3.04 | 2.54 |
| 1255.5 | 2.36E-04 | 9.56E-07 | 3.32 | 1.98 |
| 1255.5 | 2.21E-04 | 8.97E-07 | 3.85 | 1.07 |
| 1255.5 | 3.23E-04 | 1.31E-06 | 4.05 | 0.76 |

MacMullin geometry correction

EIS measurements made following the bulk impedance section in Hou and Monroe [1] with this equation:

κeff=LΩbulkA   ,		           			(S4)

Where Ωbulk is the bulk impedance measured with EIS, L is the PEEK spacer thickness (0.2 cm) and A is the PEEK spacer cross sectional area (0.503 cm2).

The MacMullin number α depends on pore geometry and is found by scaling the effective conductivity κeff with the pure liquid electrolyte conductivity κ:

α=κeffκ  .						(S5)

By taking the manufacturer specification for porosity ε=0.85, one may then calculate the Bruggeman exponent b based on effective medium theory via:

α=εb .						(S6)

Figure S1 reports the spread in b, and an average of b = 1.23 with a standard deviation of 0.74 is found. This wide variability in the Bruggeman exponent suggests a correspondingly wide variability in the pore structure of the glass fiber.

Figure S2. Bruggeman exponent b (x) calculated for each individual restricted-diffusion measurement for LiPF6:EMC. An average value of 1.23 with standard deviation 0.74 is indicated (- - -).

Figure S3. Individual voltage relaxation data from all restricted diffusion measurements for LiPF6:EMC. Dashed lines (- - -) indicate region of slope used to compute Deff.

Table S9. Parameters and 95% confidence intervals to accompany correlations presented in table 2 from main text.

| Electrolyte | Property | T / °C | Fit parameters & confidence intervals |  |  |
| --- | --- | --- | --- | --- | --- |
| LiPF6:EMC | ρ(c [M]) | 20 | 1013.1 | 113.19 | -7.8842 |
|  |  |  | — | ±2.70 | ±1.998 |
|  |  | 25 | 1007.1 | 114.20 | -8.1212 |
|  |  |  | — | ±2.80 | ±2.029 |
|  |  | 30 | 1001.1 | 115.13 | -8.3005 |
|  |  |  | — | ±2.70 | ±2.04 |
|  | η(y) | 20 | 0.724 | 43.80 | 5.964×105 |
|  |  |  | — | ±1.02 | ±8800 |
|  |  | 25 | 0.680 | 36.01 | 5.655×105 |
|  |  |  | — | ±4.2000 | ±36500 |
|  |  | 30 | 0.639 | 32.17 | 4.917×105 |
|  |  |  | — | ±4.49 | ±39000 |
|  | Λ(y) | 20 | -9.273 | 33.39 | -58.50 |
|  |  |  | ±0.558 | ±1.336 | ±1.981 |
|  |  | 25 | -9.631 | 34.46 | -59.64 |
|  |  |  | ±0.600 | ±1.437 | ±2.125 |
|  |  | 30 | -9.970 | 35.47 | -60.66 |
|  |  |  | ±0.602 | ±1.442 | ±2.127 |
|  | χEMC(y) | 25 | 1 | -18.38 | 155.3 |
|  |  |  | — | ±4.330 | ±48.35 |
|  | t+0(y) | 25 | 0.4240 | -1.858 | 4.880 |
|  |  |  | ±0.020 | ±0.467 | ±2.179 |
|  | D(y) | 25 | 504.8 | -6.064 | 11.35 |
|  |  |  | ±27.05 | ±1.417 | ±7.345 |

Table S9. Continued Parameters and 9% confidence intervals to accompany correlations presented in table 2 from main text.

| Electrolyte | Property | T / °C | Fit parameters & confidence intervals |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| LiPF6:PC | η(y) | 20 | 2.74 |  | 287.9 |  | 1.702×107 |  |
|  |  |  | ±0.353 |  | ±22.15 |  | ±545000 |  |
|  |  | 25 | 2.47 |  | 246.7 |  | 1.245×107 |  |
|  |  |  | ±0.234 |  | ±14.75 |  | ±365000 |  |
|  |  | 30 | 2.24 |  | 212.3 |  | 9.382×106 |  |
|  |  |  | ±0.184 |  | ±11.50 |  | ±283000 |  |
|  | χPC(y) | 25 | 1 | -2.655 |  | 26.23 |  | 1490 |
|  |  |  | — | ±1.209 |  | ±5.075 |  | ±336.5 |