The files available here contain the following data:

| File | contents |
| --- | --- |
| Zr microcantilever composition data.xlsx | Chemical composition of the Zr sample [Excel xlsx format] |
| Zr microcantilever optical micrograph.tif | Optical micrograph showing grain structure revealed by use of cross-polars. Also seen in the image is an array of nano-indents |
| Zr microcantilever SEM example cantilever.tif | SEM image showing the triangular cross-section shape of the micro-cantilevers used. This example is 5 µm wide and 30 µm long. The aspect ratio was maintained for other micro-cantilever sizes. |
| Zr microcantilever constitutive equation constants.xlsx | Constants for constitutive equation used in crystal plasticity modelling of load-displacement data. [Excel xlsx format] |
| Zr microcantilever load displacement data.xlsx | Load-displacement data for each micro-cantilever (different orientations and sizes) as measured in the experiments along with the best fit crystal plasticity finite element simulation results. [Excel xlsx format] |
| Zr microcantilever CRSS vs size data.xlsx | critical resolved shear stress (CRSS) required for best fit to load-displacement data as a function of micro-cantilever size for each of three slip systems. [Excel xlsx format] |
| Zr microcantilever bulk CRSS vs slip system.xlsx | CRSS values for three slip systems extrapolated to bulk size. [Excel xlsx format] |
| Zr bulk EBSD grain orientations | Crystal orientation data obtained from EBSD measurement. Orientations given through three Euler angles (Bunge notation), along with grain centroid position for 730 grains. [text file – grain file output from TSL OIM software] |
| Zr bulk compression load displacement data.xlsx | Stress-strain data from compression testing of polycrystalline Zr sample. Stress-strain results obtained from crystal plasticity simulation using bulk CRSS values and measured grain orientations in included. [Excel xlsx format] |