Supporting Information

Group 4 constrained geometry complexes for olefin (co)polymerisation

Thomas J. Williams, Alexander D. H. Smith, Jean-Charles Buffet, Zoë R. Turner and Dermot O'Hare*

Chemistry Research Laboratory, Department of Chemistry, University of Oxford, 12 Mansfield Road, OX1 3TA, UK

Corresponding author: dermot.ohare@chem.ox.ac.uk

Table of Contents

1. Experimental techniques, physical methods and synthesis					S2

1.1 General procedure and physical methods						S2

1.2 Additional experimental synthetic data						S4

2. NMR spectroscopy										S9

2.1 Solution NMR spectroscopy							S9

2.2 Solid-state NMR spectroscopy							S23

3. Additional ethylene polymerisation data							S32

4. Additional X-ray crystallography data							S50

4.1 Experimental crystallographic data 						S50

5. References											S52

# Experimental techniques, physical methods and synthesis

1.1 General procedures and physical methods.

General procedures. Air- and moisture-sensitive techniques were undertaken in an inert atmosphere of nitrogen, using standard Schlenk techniques, on a dual manifold nitrogen/vacuum line or in an MBraun Unilab glovebox. Pentane, hexane, toluene and benzene were dried using an MBraun SPS 800 solvent purification system. Tetrahydrofuran (THF) and diethyl ether were distilled from purple Na/benzophenone. Tert-butylamine and cyclohexylamine were dried over CaH2 and then freeze-pump-thaw degassed three times. The amines and THF were stored over pre-activated 3 Å molecular sieves; hexane, pentane, benzene and toluene were stored on a potassium mirror. Deuterated solvents were dried over potassium (C6D6) or CaH2 (C5D5N), freeze-pump-thaw degassed, vacuum transferred and stored over pre-activated 4 Å molecular sieves. I*SiMe2Cl was synthesised using a literature procedure from hexamethylindene (Ind#H).1 Lithium amides were prepared via lithiation of an amine with 1.1 equivalents of nBuLi. TiCl4·2THF was synthesised via a literature procedure from TiCl4.2

Solution phase NMR spectroscopy. NMR spectra were recorded on either a 400 MHz Bruker Avance III HD nanobay spectrometer or a 500 MHz Bruker Avance III HD nanobay spectrometer. 1H and 13C{1H} NMR spectra were recorded at 298 K unless otherwise stated, referenced internally to the residual protio-solvent resonance in the deuterated solvent. Air-sensitive samples were prepared in a glovebox under an inert atmosphere, using dried deuterated solvents in Young’s tap NMR tubes.

Solid-state NMR spectroscopy. All experiments were carried out by Dr. Nicholas Rees (University of Oxford). Compounds were prepared in a glovebox under a nitrogen atmosphere and sealed in 5 mm zirconia rotors. Spectra were recorded on a Bruker Avance III HD NanoBay 400.2 MHz Solid-state NMR spectrometer, samples were spun at the magic angle (54.71°) at spin rates 10 kHz for 13C CP-MAS, 27Al DP-MAS, and 29Si CP-MAS. 13C NMR spectra were referenced to adamantane, 27Al to Al(NO3)3.

X-ray crystallography. X-ray crystallography was carried out by Dr. Zöe Turner (University of Oxford). Crystals were mounted on MiTeGen MicroMounts using perfluoropolyether oil and rapidly transferred to a goniometer head on a diffractometer fitted with an Oxford Cryosystems Cryostream open-flow nitrogen cooling device.3 Data collections were carried out at 150 K using an Oxford Diffraction Supernova diffractometer using mirror-monochromated Cu Kα radiation (λ = 1.54178 Å) and data were processed using CrysalisPro.4 The structures were solved using direct methods (SIR-92)5 or a charge flipping algorithm (SUPERFLIP)6 and refined by full-matrix least-squares procedures using the Win-GX software suite.7 Solid state structural data have been deposited in the Cambridge Crystallographic Data Centre (1966405-1966407).

Elemental analysis. Samples were prepared in a glovebox and analysed by Mr Stephen Boyer (London Metropolitan University).

Differential scanning calorimetry (DSC). Samples were run on a DSC3+ (Mettler Toledo, Ltd) using 5 mg of polymer in a sealed aluminium 100 μL crucible. An empty crucible was used as a reference, and the DSC was calibrated using indium. Samples were heated from 25 to 250 °C and cooled back again at a rate of 5 °C per minute, a total of three cycles were run. Polymer melt temperature values were taken from the third heating cycle.

1.2 Additional experimental synthetic data.

### Synthesis of 3-EtI*SiMe2Cl

3-EtI*Li (2.00 g, 9.07 mmol) was dissolved in THF. This was then added dropwise to a THF solution of three equivalents of SiMe2Cl2 (3.28 mL, 27.2 mmol) and the reaction mixture was stirred for 3 hours at 23 °C. The volatiles were removed under vacuum and the product was extracted in pentane. The solution was concentrated and a yellow solid precipitated at −20 °C. The solid melted to form a yellow oil at room temperature and was isolated in 83% yield (2.30 g, 7.49 mmol).

1H NMR (C6D6, 298 K, 400 MHz): δ (ppm) 3.50 (1H, s, I*H), 2.66 (2H, m, I*-CH2-CH3), 2.44 (3H, s, I*-Me), 2.14 (3H, s, I*-Me), 2.13 (3H, s, I*-Me), 2.12 (3H, s, I*-Me), 2.12 (3H, s, I*-Me), 1.13 (3H, dd, I*-CH2-CH3, 3JH-H = 7.5 Hz, 3JH-H = 7.5 Hz), 0.20 (3H, s, Si-Me), −0.08 (3H, s, Si-Me).

### Synthesis of Me2SB(tBuN,3-EtI*)H2

3-EtI*SiMe2Cl (1.16 g, 3.78 mmol) was added to 1.05 equivalents of LiN(H) tBu (0.310 g, 3.97 mmol), and the mixture was cooled in an ice bath. THF (30 ml) was added, and the reaction mixture was allowed to warm to 23 °C and stirred for 2 hours. The volatiles were removed under vacuum and the product then extracted in pentane. The solution was dried in vacuo to yield Me2SB(tBuN,3-EtI*)H2 a pale yellow oil in a quantitative yield.

1H NMR (C6D6, 298 K, 400 MHz): δ (ppm) 3.32 (1H, s, I*H), 2.77 (2H, m, I*-CH2-CH3), 2.52 (3H, s, I*-Me), 2.30 (3H, s, I*-Me), 2.22 (3H, s, I*-Me), 2.19 (3H, s, I*-Me), 2.13 (3H, s, I*-Me), 1.24 (3H, dd, I*-CH2-CH3, 3JH-H = 7.5 Hz, 3JH-H = 7.5 Hz), 1.08 (9H, s, N-tBu), 0.47 (1H, s, N-H), 0.16 (3H, s, Si-Me) and −0.13 (3H, s, Si-Me). 13C{1H} NMR (C6D6, 298 K, 125 MHz): δ (ppm) 143.03 (I*), 140.91 (I*), 140.20 (I*), 138.59 (I*), 132.03 (I*), 129.50 (I*), 127.01 (I*), 125.64 (I*), 50.15 (I*-Si), 49.54 (N-C-(CH3)3), 33.85 (N-C-(CH3)3), 21.26 (I*-CH2-CH3), 19.51 (I*-Me), 16.50 (I*-Me)16.44 (I*-Me), 16.13 (I*-Me), 15.37 (I*-Me), 15.19 (I*-CH2-CH3), 3.71 (Si-Me) and 0.22 (Si-Me).

### Synthesis of Me2SB(tBuN,3-EtI*)Li2.1.5THF

Me2SB(tBuN,3-EtI*)H2 (1.30 g, 3.78 mmol) was dissolved in THF (30 mL) and cooled to 5 °C. 2.2 equivalents of nBuLi (1.6 M in hexanes; 5.2 mL, 8.32 mmol) was added dropwise to the solution and the reaction mixture allowed to warm to 23 °C and was stirred for 30 minutes. The mixture was dried under vacuum and the residue was washed with cold pentane (4 x 25 mL). The resulting pale yellow solid was then dried in vacuo to yield Me2SB(tBuN,3-EtI*)Li2.1.5THF in a 43% yield (0.760 g, 1.64 mmol)

1H NMR (C6D5N, 298 K, 400 MHz): δ (ppm) 3.68 (6H, m, O-CH2-CH2), 3.43 (2H, quartet, I*-CH2-CH3, 3JH-H =7.2 Hz), 3.19 (3H, s, I*-Me), 3.02 (3H, s, I*-Me), 2.93 (3H, s, I*-Me), 2.53 (3H, s, I*-Me), 2.52 (3H, s, I*-Me), 3.68 (6H, m, O-CH2-CH2), 1.47 (3h, t, I*,-CH2-CH3, 3JH-H =7.2 Hz), 1.38 (9H, s, N-tBu) and 0.82 (6H, s, Si-Me2). 7Li NMR (C6D5N, 298 K, 155.5 MHz): δ (ppm) 1.84.

### Synthesis of Me2SB(CyN,I*)H2

I*SiMe2Cl (2.00 g, 6.82 mmol) was mixed with an equimolar amount of LiN(H)Cy (0.720 g, 6.82 mmol) and cooled to 5 °C. The mixture was dissolved in THF, allowed to warm to 23 °C and stirred for 2 hours. The reaction mixture was dried under vacuum and the product extracted in pentane as a pale yellow solution. The pentane was removed in vacuo to yield Me2SB(CyN,I*)H2 as a yellow oil in quantitative yield.

1H NMR (C6D6, 298 K, 400 MHz): δ (ppm) 3.35 (1H, s, I*-H), 2.53 (3H, s, I*-Me), 2.45 (1H, m, N-CyHipso), 2.30 (3H, s, I*-Me), 2.30 (3H, s, I*-Me), 2.22 (3H, s, I*-Me), 2.20 (3H, s, I*-Me), 2.08 (3H, s, I*-Me), 1.71 (2H, m, N-CyHortho), 1.58 (2H, m, N-CyHmeta), 1.46 (1H, m, N-CyHpara), 1.14 (2H, m, N-CyHmeta), 1.03 (1H, m, N-CyHpara), 0.89 (2H, m, N-CyHortho), 0.26 (1H, m, N-H), 0.08 (3H, s, Si-Me) and −0.08 (3H, s, Si-Me). 13C{1H} NMR (C6D6, 298 K, 125 MHz): δ (ppm) 142.60 (I*), 142.00 (I*), 139.73 (I*), 132.20 (I*), 131.82 (I*), 129.53 (I*), 126.78 (I*), 126.09 (I*), 51.01 (N-Cyipso), 50.24 (I*-Si), 38.95 (N-Cyortho), 38.86 (N-Cyortho), 26.19 (N-Cypara), 25.88 (2 x N-Cymeta), 19.34 (I*-Me), 16.51 (I*-Me), 16.40 (I*-Me), 16.37 (I*-Me), 15.65 (I*-Me), 13.37 (I*-Me), −0.84 (Si-Me) and −1.18 (Si-Me).

### Synthesis of Me2SB(CyN,I*)Li2

Me2SB(CyN,I*)H2 (2.43 g, 6.82 mmol) was dissolved in THF and then cooled in an ice bath. 2.2 equivalents of nBuLi (1.6 M in hexanes; 9.38 mL, 15.0 mmol) was added dropwise, and the reaction mixture allowed to warm to 23 °C and stirred for 30 minutes. The reaction mixture was dried under vacuum and the dark yellow solid product was washed with cold pentane (4x25 mL) to yield Me2SB(CyN,I*)Li2 as a pale yellow solid in 48% yield (3.27 mmol). 1H NMR (C6D5N, 298 K, 400 MHz): δ (ppm)  3.17 (3H, s, I*-Me), 3.13 (1H, m, N-Cy), 3.07 (3H, s, I*-Me), 3.05 (3H, s, I*-Me), 2.87 (3H, s, I*-Me), 2.51 (3H, s, I*-Me), 2.51 (3H, s, I*-Me), 2.13 (2H, m, N-Cy), 1.67 (2H, m, N-Cy), 1.47 (1H, m, N-Cy), 1.26 (4H, m, N-Cy), 1.11 (1H, m, N-Cy) and 0.79 (6H, s, Si-Me). 7Li NMR (C6D5N, 298 K, 155.5 MHz): δ (ppm) 2.21.

### Synthesis of I*SiMePrCl

Ind#Li (5.00 g, 24.3 mmol) was dissolved in THF (25 mL) and added dropwise over 30 minutes to a solution of 1.5 equivalents of SiMePrCl2 (5.46 mL, 36.5 mmol) in THF at 23 °C. The reaction mixture was stirred for 3 hours and the volatiles were removed under vacuum. The product was extracted in pentane as a pale orange solution, the solution was concentrated and I*SiMePrCl precipitated as a pale orange solid at −20 °C in a 73% yield (7.28 g, 17.4 mmol) as two isomers.

1H NMR (C6D6, 298 K, 500 MHz): δ (ppm) 3.55 (1H, s, I*-H), 1.29 (2H, s, Si-CH2-CH2-CH3), 0.75 (3H, t, Si-CH2-CH2-CH3), 0.53 (2H, m, Si-CH2-CH2-CH3), 0.21 (3H, s, Si-Me). 3.52 (1H, s, I*-H), 1.09 (2H, m, Si-CH2-CH2-CH3), 0.80 (3H, t, Si-CH2-CH2-CH3), 0.32 (2H, m, Si-CH2-CH2-CH3), −0.01 (3H, s, Si-Me). 2.44 (6H, s, I*-Me), 2.22 (3H, s, I*-Me), 2.19 (3H, s, I*-Me), 2.18 (6H, s, I*-Me), 2.13 (6H, s, I*-Me), 2.12 (6H, s, I*-Me), 2.11 (3H, s, I*-Me) and 2.09 (3H, s, I*-Me). Resonances cannot be specifically assigned to either isomer.

### Synthesis of Me,PrSB(tBuN,I*)H2

I*SiMePrCl (2.00 g, 6.23 mmol) was added to 1.05 equivalents of LiN(H)tBu (0.520 g, 6.59 mmol) and the mixture was cooled to 5 °C. THF (30 mL) was added and the reaction mixture was allowed to warm to 23 °C and stirred for 2 hours. The volatiles were removed under vacuum and the product extracted in pentane as a pale yellow solution. The mixture was dried in vacuo to yield Me,PrSB(tBuN,I*)H2, a dark yellow oil, in a quantitative yield.

1H NMR (C6D6, 298 K, 500 MHz): δ (ppm) 2.53 (6H, s, I*-Me), 2.33 (6H, s, I*-Me), 2.30 (6H, s, I*-Me), 2.22 (6H, s, I*-Me), 2.18 (6H, s, I*-Me), 2.14 (3H, s, I*-Me), 2.11 (3H, s, I*-Me). Major Isomer (55%): δ (ppm) 3.45 (1H, s, I*-H), 1.14 (2H, m, Si-CH2-CH2-CH3), 1.11 (9H, s, N-tBu), 0.87 (3H, t, Si-CH2-CH2-CH3, 3JH-H = 7.12), 0.68 (2H, m, Si-CH2-CH2-CH3), 0.41 (1H, s, N-H), 0.18 (3H, s, Si-Me). Minor isomer (45%): δ (ppm) 3.41 (1H, s, I*-H), 1.22 (2H, m, Si-CH2-CH2-CH3), 1.06 (9H, s, N-tBu), 0.93 (3H, t, Si-CH2-CH2-CH3, 3JH-H = 7.36), 0.57 (2H, m, Si-CH2-CH2-CH3), 0.36 (1H, s, N-H) and −0.02 (3H, s, Si-Me).

### Synthesis of Me,PrSB(tBuN,I*)Li2

Me,PrSB(tBuN,I*)H2 (2.23 g, 6.23 mmol) was dissolved in THF and cooled in an ice bath. 2.2 equivalents of nBuLi (1.6 M in hexanes; 8.60 mL, 13.7 mmol) was added dropwise, and the reaction mixture allowed to warm to 23 °C and stirred for 30 minutes. The reaction mixture was dried under vacuum and the dark yellow solid was washed with cold pentane (4 x 25 mL) to yield Me,PrSB(tBuN,I*)Li2.1.2THF as a pale yellow solid in 31% yield (1.93 mmol).

1H NMR (C6D5N, 298 K, 500 MHz): δ (ppm) 3.69 ( 4.8H, m, O-CH2-CH2), 3.20 (3H, s, I*-Me), 2.05 (3H, s, I*-Me), 3.05 (3H, s, I*-Me), 2.90 (3H, s, I*-Me), 2.52 (3H, s, I*-Me), 2.50 (3H, s, I*-Me), 1.70 (2H, m, CH2-CH2-CH3), 1.65 ( 4.8H, m, O-CH2-CH2), 1.40 (9H, s, N-tBu), 1.25 (2H, m, CH2-CH2-CH3), 1.06 (3H, m, CH2-CH2-CH3) and 0.84 (3H, s, Si-Me). 7Li NMR (C6D5N, 298 K, 155.5 MHz): δ (ppm) 2.21.

# NMR Spectroscopy

## 2.1 Solution NMR Spectroscopy

Figure S2.1. 1H NMR spectrum (C6D6, 298 K, 500 MHz) of Me2SB(tBuN,I*)TiMe2. Solvent resonance omitted for clarity.

Figure S2.2. 1H NMR spectrum (C6D6, 298 K, 500 MHz) of Me2SB(tBuN,I*)Ti(CH2Ph)2 .

Figure S2.3. 13C{1H} NMR spectrum (C6D6, 298 K, 125 MHz) of Me2SB(tBuN,I*)Ti(CH2Ph)2.

Figure S2.4. 1H NMR spectrum (C6D6, 298 K, 500 MHz) of Me2SB(tBuN,I*)Ti(CH2SiMe3)2.

Figure S2.5. 13C{1H} NMR spectrum (C6D6, 298 K, 125 MHz) of Me2SB(tBuN,I*)Ti(CH2SiMe3)2.

Figure S2.6. 1H NMR spectrum (C6D6, 298 K, 500 MHz) of Me2SB(tBuN,I*)Ti(Cl)CH2SiMe3.

Figure S2.7. 13C{1H} NMR spectrum (C6D6, 298 K, 125 MHz) of Me2SB(tBuN,I*)Ti(Cl)CH2SiMe3.

Figure S2.8. 1H NMR spectrum (C6D6, 298 K, 500 MHz) of Me2SB(CyN,I*)H2. Solvent resonance omitted for clarity.

Figure S2.9. 13C{1H} NMR spectrum (C6D6, 298 K, 125 MHz) of Me2SB(CyN,I*)H2.

Figure S2.10. 1H NMR spectrum (C6D5N, 298 K, 500 MHz) of Me2SB(CyN,I*)Li2.

Figure S2.11. 1H NMR spectrum (C6D6, 298 K, 500 MHz) of Me2SB(CyN,I*)TiCl2. Solvent resonance omitted for clarity.

Figure S2.12. 13C{1H} NMR spectrum (C6D6, 298 K, 125 MHz) of Me2SB(CyN,I*)TiCl2.

Figure S2.13. 1H NMR spectrum (C6D6, 298 K, 400 MHz) of 3-EtI*SiMe2Cl. Solvent resonance omitted for clarity.

Figure S2.14. 1H NMR spectrum (C6D6, 298 K, 400 MHz) of Me2SB(tBuN,3-EtI*)H2. Solvent resonance omitted for clarity.

Figure S2.15. 13C{1H} NMR spectrum (C6D6, 298 K, 125 MHz) of Me2SB(tBuN,3-EtI*)H2.

Figure S2.16. 1H NMR spectrum (C6D5N, 298 K, 400 MHz) of Me2SB(tBuN,3-EtI*)Li2. Solvent resonances omitted for clarity.

Figure S2.17. 1H NMR spectrum (C6D6, 298 K, 400 MHz) of  Me2SB(tBuN,3-EtI*)TiCl2. Solvent resonance omitted for clarity.

Figure S2.18. 13C{1H} NMR spectrum (C6D6, 298 K, 125 MHz) of Me2SB(tBuN,3-EtI*)TiCl2.

Figure S2.19. 1H NMR spectrum (C6D6, 298 K, 400 MHz) of I*SiMePrCl. Solvent resonance omitted for clarity.

Figure S2.20.  1H NMR spectrum (C6D6, 298 K, 400 MHz) of Me,PrSB(tBuN,I*)H2. Solvent resonance omitted for clarity.

Figure S2.21. 1H NMR spectrum (C6D5N, 298 K, 400 MHz) of Me,PrSB(tBuN,I*)Li2. Solvent resonances omitted for clarity.

Figure S2.22. 1H NMR spectrum (C6D6, 298 K, 500 MHz) of Me,PrSB(tBuN,I*)TiCl2. Solvent resonance omitted for clarity.

Figure S2.23. 13C{1H} NMR spectrum (C6D6, 298 K, 125 MHz) of Me,PrSB(tBuN,I*)TiCl2.

Figure S2.24. 1H NMR spectrum (C6D6, 298 K, 400 MHz) of Me2SB(tBuN,I*)ZrCl2. Solvent resonance omitted for clarity, resonances at 1.22 and 0.88 ppm correspond to residual pentane.

Figure S2.25.  13C{1H} NMR spectrum (C6D6, 298 K, 125 MHz) of Me2SB(tBuN,I*)ZrCl2.

Figure S2.26. 1H NMR spectrum (C6D6, 298 K, 400 MHz) of the reaction of Me2SB(tBuN,I*)TiCl2 with from bottom to top: 0, 1, 2, 5 and 10 equivalents of MAO.

## Solid State NMR Spectroscopy

Figure S2.27. 13C CP-MAS (100.6 MHz) NMR spectrum of sMAO-Me2SB(tBuN,I*)TiMe2.

Figure S2.28. 27Al DP-MAS hahnecho (104.2 MHz) NMR spectrum of sMAO-Me2SB(tBuN,I*)TiMe2.

Figure S2.29. 29Si CP-MAS (79.4 MHz) NMR spectrum of sMAO-Me2SB(tBuN,I*)TiMe2.

Figure S2.30. 13C CP-MAS (100.6 MHz) NMR spectrum of sMAO-Me2SB(tBuN,I*)Ti(CH2Ph)2.

Figure S2.31. 27Al DP-MAS hahnecho (104.2 MHz) NMR spectrum of sMAO-Me2SB(tBuN,I*)Ti(CH2Ph)2.

Figure S2.32. 29Si CP-MAS (79.4 MHz) NMR spectrum of sMAO-Me2SB(tBuN,I*)Ti(CH2Ph)2.

Figure S2.33. 13C CP-MAS (100.6 MHz) NMR spectrum of sMAO-Me2SB(tBuN,I*)Ti(Cl)CH2SiMe3.

Figure S2.34. 27Al DP-MAS hahnecho (104.2 MHz) NMR spectrum of sMAO-Me2SB(tBuN,I*)Ti(Cl)CH2SiMe3.

Figure S2.35. 29Si CP-MAS (79.4 MHz) NMR spectrum of sMAO-Me2SB(tBuN,I*)Ti(Cl)CH2SiMe3.

Figure S2.36. 13C CP-MAS (100.6 MHz) NMR spectrum of sMAO-Me2SB(tBuN,I*)Ti(CH2SiMe3)2.

Figure S2.37. 27Al DP-MAS hahnecho (104.2 MHz) NMR spectrum of sMAO-Me2SB(tBuN,I*)Ti(CH2SiMe3)2.

Figure S2.38. 29Si CP-MAS (79.4 MHz) NMR spectrum of sMAO-Me2SB(tBuN,I*)Ti(CH2SiMe3)2.

Figure S2.39. 13C CP-MAS (100.6 kHz) NMR spectrum of sMAO-Me2SB(tBuN,Cp*)TiCl2.

Figure S2.40. 27Al DP-MAS hahnecho (104.2 kHz) NMR spectrum of sMAO-Me2SB(tBuN,Cp*)TiCl2.

Figure S2.41. 29Si CP-MAS (79.4 MHz) NMR spectrum of sMAO-Me2SB(tBuN,Cp*)TiCl2.

Figure S2.42. 13C CP-MAS (100.6 kHz) NMR spectrum of sMAO-Me2SB(tBuN,3-EtI*)TiCl2.

Figure S2.43. 27Al DP-MAS hahnecho (104.2 kHz) NMR spectrum of sMAO-Me2SB(tBuN,3-EtI*)TiCl2.

Figure S2.44. 29Si CP-MAS (79.4 MHz) NMR spectrum of sMAO-Me2SB(tBuN,3-EtI*)TiCl2.

# Additional ethylene polymerisation data

Table S3.1. Polymerisation activities, mass of catalyst used, and mass of polymer produced. Polymerisation conditions: 10 mg catalyst, 2 bar ethylene, 50 mL hexane, 150 mg TiBA and 30 minutes.

| Temperature (°C) | Mass Catalyst (mg) |  | Mass Polymer (g) |  | Activity (kgPE/molTi/h/bar) |  | Average Activity (kgPE/molTi/h/bar) |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | A | B | A | B | A | B |  |
| sMAO-Me2SB(tBuN,I*)TiCl2 |  |  |  |  |  |  |  |
| 50 | 9.9 | 10.2 | 2.216 | 2.530 | 2806 | 3110 | 2958 |
| 60 | 9.8 | 10.1 | 2.743 | 2.977 | 3509 | 3696 | 3602 |
| 70 | 9.8 | 9.8 | 2.602 | 2.907 | 3328 | 3719 | 3524 |
| 80 | 10.3 | 10.1 | 2.354 | 2.495 | 2865 | 3097 | 2981 |
| 90 | 9.8 | 10.1 | 1.984 | 2.088 | 2538 | 2592 | 2565 |
| sMAO-Me2SB(tBuN,I*)Ti(CH2Ph)2 |  |  |  |  |  |  |  |
| 50 | 10.0 | 10.3 | 3.70 | 3.87 | 5651 | 5739 | 5695 |
| 60 | 9.9 | 9.5 | 3.55 | 3.80 | 5477 | 6109 | 5793 |
| 70 | 10.2 | 10.1 | 3.97 | 3.71 | 5945 | 5610 | 5777 |
| 80 | 9.5 | 9.8 | 3.18 | 3.36 | 5112 | 5236 | 5174 |
| 90 | 9.7 | 10.0 | 2.37 | 2.71 | 3732 | 4139 | 3935 |
| sMAO-Me2SB(tBuN,I*)TiMe2 |  |  |  |  |  |  |  |
| 50 | 10.2 | 9.7 | 4.42 | 4.42 | 4937 | 5191 | 5064 |
| 60 | 10.2 | 10.0 | 4.77 | 4.76 | 5328 | 5423 | 5375 |
| 70 | 10.3 | 9.6 | 4.37 | 4.23 | 4834 | 5020 | 4927 |
| 80 | 10.0 | 10.3 | 3.61 | 3.45 | 4113 | 3816 | 3964 |
| 90 | 10.0 | 10.2 | 2.44 | 2.75 | 2780 | 3072 | 2926 |
| sMAO-Me2SB(tBuN,I*)Ti(CH2SiMe3)2 |  |  |  |  |  |  |  |
| 50 | 10.1 | 10.0 | 4.54 | 4.63 | 6944 | 7152 | 7048 |
| 60 | 10.5 | 10.0 | 4.64 | 4.47 | 6826 | 6905 | 6866 |
| 70 | 10.0 | 10.0 | 3.98 | 4.01 | 6148 | 6195 | 6171 |
| 80 | 10.4 | 9.9 | 3.07 | 2.57 | 4560 | 4010 | 4285 |
| 90 | 10.0 | 10.0 | 1.26 | 1.30 | 1946 | 2008 | 1977 |
| sMAO-Me2SB(tBuN,I*)Ti(Cl)SiMe3 |  |  |  |  |  |  |  |
| 50 | 10.4 | 10.4 | 1.863 | 1.748 | 2506 | 2351 | 2429 |
| 60 | 10.5 | 10.7 | 2.085 | 2.376 | 2778 | 3107 | 2943 |
| 70 | 10.1 | 9.5 | 1.730 | 1.641 | 2397 | 2416 | 2407 |
| 80 | 9.3 | 9.5 | 1.104 | 0.916 | 1661 | 1349 | 1505 |
| 90 | 10.0 | 10.0 | 0.618 | 0.616 | 865 | 862 | 863 |
| sMAO-Me2SB(CyN,I*)TiCl2 |  |  |  |  |  |  |  |
| 50 | 10.4 | 10.1 | 0.557 | 0.514 | 808 | 768 | 788 |
| 60 | 9.8 | 10.0 | 0.477 | 0.506 | 735 | 764 | 749 |
| 70 | 9.6 | 9.6 | 0.464 | 0.494 | 730 | 777 | 753 |
| 80 | 9.8 | 10.0 | 0.402 | 0.457 | 619 | 690 | 655 |
| 90 | 10.2 | 10.1 | 0.228 | 0.216 | 337 | 323 | 330 |
| sMAO-Me,PrSB(tBuN,I*)TiCl2 |  |  |  |  |  |  |  |
| 50 | 10.1 | 10.3 | 2.899 | 3.292 | 3954 | 4403 | 4178 |
| 60 | 9.7 | 10.0 | 2.988 | 3.013 | 4243 | 4151 | 4197 |
| 70 | 10.0 | 10.1 | 2.939 | 3.100 | 4049 | 4228 | 4138 |
| 80 | 9.9 | 10.2 | 2.329 | 2.100 | 3241 | 2836 | 3038 |
| 90 | 10.2 | 10.1 | 1.965 | 1.938 | 2680 | 2617 | 2649 |
| sMAO-Me2SB(tBuN,3-EtI*)TiCl2 |  |  |  |  |  |  |  |
| 50 | 10.5 | 10.5 | 3.134 | 3.470 | 3860 | 4272 | 4067 |
| 60 | 9.6 | 9.8 | 2.825 | 3.047 | 38.05 | 4021 | 3913 |
| 70 | 9.6 | 9.4 | 2.750 | 2.531 | 3704 | 3482 | 3593 |
| 80 | 9.6 | 9.6 | 2.034 | 1.972 | 2740 | 2656 | 2698 |
| 90 | 10.0 | 10.4 | 1.948 | 1.710 | 2519 | 2126 | 2323 |
| sMAO-Me2SB(tBuN,I*)ZrCl2 |  |  |  |  |  |  |  |
| 50 | 10.6 | 10.1 | 0.078 | 0.085 | 105 | 120 | 112 |
| 60 | 9.7 | 9.7 | 0.068 | 0.064 | 100 | 94 | 97 |
| 70 | 9.5 | 9.5 | 0.068 | 0.071 | 102 | 106 | 104 |
| 80 | 9.6 | 10.5 | 0.048 | 0.062 | 71 | 84 | 78 |
| 90 | 9.5 | 9.5 | 0.062 | 0.057 | 83 | 85 | 89 |

Table S3.2. Polymerisation activities, mass of catalyst used, and mass of polymer produced. Polymerisation conditions: 10 mg catalyst, 2 bar ethylene, 50 mL hexane, 150 mg TiBA and 30 minutes.

| Time (minutes) | Mass Catalyst (mg) |  | Mass Polymer (g) |  | Activity (kgPE/molTi/h/bar) |  | Average Activity (kgPE/molTi/h/bar) |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | A | B | A | B | A | B |  |
| sMAO-Me2SB(tBuN,I*)TiCl2 |  |  |  |  |  |  |  |
| 5 | 9.6 | 9.8 | 0.677 | 0.758 | 5305 | 5819 | 5562 |
| 15 | 10.0 | 9.9 | 1.871 | 1.764 | 4692 | 4468 | 4580 |
| 30 | 9.8 | 9.8 | 2.602 | 2.907 | 3328 | 3719 | 3524 |
| 60 | 9.8 | 9.8 | 4.495 | 4.801 | 2875 | 3071 | 2973 |
| sMAO-Me2SB(tBuN,I*)Ti(CH2Ph)2 |  |  |  |  |  |  |  |
| 5 | 10.1 | 9.8 | 1.20 | 1.24 | 10888 | 11595 | 11241 |
| 15 | 10.3 | 10.5 | 2.65 | 2.72 | 7859 | 7913 | 7886 |
| 30 | 10.2 | 10.1 | 3.97 | 3.71 | 5945 | 5610 | 5777 |
| 60 | 10.0 | 10.5 | 6.13 | 6.1 | 4681 | 4436 | 4559 |
| sMAO-Me2SB(tBuN,I*)TiMe2 |  |  |  |  |  |  |  |
| 5 | 10.4 | 9.7 | 1.37 | 1.25 | 9004 | 8809 | 8907 |
| 15 | 10.2 | 9.7 | 2.79 | 2.54 | 6232 | 5966 | 6099 |
| 30 | 10.3 | 9.6 | 4.37 | 4.23 | 4834 | 5020 | 4927 |
| 60 | 10.0 | 9.7 | 6.98 | 6.54 | 3976 | 3840 | 3908 |
| sMAO-Me2SB(tBuN,I*)Ti(CH2SiMe3)2 |  |  |  |  |  |  |  |
| 5 | 10.1 | 9.8 | 1.19 | 1.20 | 10920 | 11349 | 11135 |
| 15 | 9.7 | 9.9 | 2.42 | 2.43 | 7708 | 7583 | 7646 |
| 30 | 10.0 | 10.0 | 3.98 | 4.01 | 6148 | 6195 | 6171 |
| 60 | 10.2 | 9.8 | 5.73 | 5.47 | 4339 | 4311 | 4325 |
| sMAO-Me2SB(tBuN,I*)Ti(Cl)SiMe3 |  |  |  |  |  |  |  |
| 5 | 9.1 | 9.1 | 0.703 | 0.711 | 6485 | 6559 | 6522 |
| 15 | 10.1 | 10.1 | 1.351 | 1.373 | 3743 | 3804 | 3774 |
| 30 | 10.1 | 9.5 | 1.730 | 1.641 | 2397 | 2416 | 2407 |
| 60 | 9.7 | 9.5 | 3.034 | 3.056 | 2188 | 2250 | 2219 |
| sMAO-Me2SB(CyN,I*)TiCl2 |  |  |  |  |  |  |  |
| 5 | 10.1 | 10.2 | 0.290 | 0.305 | 2601 | 2709 | 2655 |
| 15 | 9.6 | 9.8 | 0.448 | 0.427 | 1409 | 1316 | 1362 |
| 30 | 9.6 | 9.6 | 0.464 | 0.494 | 730 | 777 | 753 |
| 60 | 9.6 | 9.4 | 0.580 | 0.501 | 456 | 402 | 429 |
| sMAO-Me,PrSB(tBuN,I*)TiCl2 |  |  |  |  |  |  |  |
| 5 | 10.5 | 10.3 | 0.901 | 0.866 | 7092 | 6949 | 7021 |
| 15 | 10.4 | 10.3 | 1.694 | 1.866 | 4488 | 4991 | 4739 |
| 30 | 10.0 | 10.1 | 2.939 | 3.100 | 4049 | 4228 | 4138 |
| 60 | 9.3 | 9.6 | 4.028 | 4.154 | 2983 | 2980 | 2982 |
| sMAO-Me2SB(tBuN,3-EtI*)TiCl2 |  |  |  |  |  |  |  |
| 5 | 10.5 | 10.5 | 0.813 | 0.814 | 6008 | 6015 | 6012 |
| 15 | 10.5 | 10.3 | 1.752 | 1.528 | 4316 | 3764 | 4040 |
| 30 | 9.6 | 9.4 | 2.750 | 2.531 | 3704 | 3482 | 3593 |
| 60 | 9.5 | 9.6 | 3.640 | 3.669 | 2478 | 2497 | 2487 |
| sMAO-Me2SB(tBuN,I*)ZrCl2 |  |  |  |  |  |  |  |
| 5 | 11.0 | 10.8 | 0.024 | 0.03 | 186 | 237 | 212 |
| 15 | 9.7 | 10.0 | 0.043 | 0.041 | 126 | 117 | 121 |
| 30 | 9.5 | 9.5 | 0.068 | 0.071 | 102 | 106 | 104 |
| 60 | 9.7 | 10.5 | 0.187 | 0.159 | 137 | 108 | 122 |

Figure S3.1. Ethylene uptake rate plots for sMAO-Me2SB(tBuN,I*)TiCl2 at 70 °C. (Co)polymerisations run for 30 minutes, 10 mg catalyst, 150 mg TiBA, 2 bar of ethylene pressure and 10 mg of catalyst. Y-axis is a guide with percentage value providing a quantitative measure of uptake.

Figure S3.2. Ethylene uptake rate plots for sMAO-Me2SB(tBuN,I*)TiCl2 at 80 °C. (Co)polymerisations run for 30 minutes, 10 mg catalyst, 150 mg TiBA, 2 bar of ethylene pressure and 10 mg of catalyst. Y-axis is a guide with percentage value providing a quantitative measure of uptake.

Figure S3.3. Ethylene uptake rate plots for sMAO-Me2SB(tBuN,I*)TiCl2 at 90 °C. (Co)polymerisations run for 30 minutes, 10 mg catalyst, 150 mg TiBA, 2 bar of ethylene pressure and 10 mg of catalyst. Y-axis is a guide with percentage value providing a quantitative measure of uptake.

Table S3.3 Polymerisation activities, mass of catalyst used, and mass of polymer produced. (Co)polymerisation conditions: 10 mg catalyst, 2 bar ethylene, 0, 0.156, 0.312 or 0.625 mL 1-hexene, 50 mL hexane, 150 mg TiBA and 30 minutes.

| Volume of 1-hexene (mL) | Mass Catalyst (mg) |  | Mass Polymer (g) |  | Activity (kgPE/molTi/h/bar) |  | Average Activity (kgPE/molTi/h/bar) |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | A | B | A | B | A | B |  |
| 30 °C |  |  |  |  |  |  |  |
| 0 | 10.0 | 10.5 | 0.985 | 0.918 | 1352 | 1200 | 1276 |
| 0.156 | 9.0 | 10.0 | 0.469 | 0.582 | 716 | 799 | 757 |
| 0.312 | 10.5 | 10.2 | 0.508 | 0.475 | 664 | 639 | 652 |
| 0.625 | 10.2 | 10.0 | 0.476 | 0.468 | 641 | 643 | 642 |
| 40 °C |  |  |  |  |  |  |  |
| 0 | 9.5 | 9.8 | 1.945 | 1.869 | 2811 | 2619 | 2715 |
| 0.156 | 9.8 | 10.2 | 1.011 | 0.911 | 1416 | 1226 | 1321 |
| 0.312 | 10.2 | 9.8 | 10.38 | 0.918 | 1397 | 1286 | 1342 |
| 0.625 | 10.5 | 10.2 | 1.166 | 1.127 | 1525 | 1517 | 1520 |
| 50 °C |  |  |  |  |  |  |  |
| 0 | 9.5 | 9.5 | 2.673 | 2.545 | 3863 | 3678 | 3771 |
| 0.156 | 10.0 | 9.6 | 1.526 | 1.357 | 2095 | 1941 | 2018 |
| 0.312 | 9.5 | 9.8 | 1.367 | 1.259 | 1976 | 1763 | 1870 |
| 0.625 | 10.2 | 9.6 | 2.311 | 2.337 | 3111 | 3343 | 3226 |
| 60 °C |  |  |  |  |  |  |  |
| 0 | 9.7 | 9.7 | 2.490 | 2.637 | 3525 | 3733 | 3629 |
| 0.156 | 9.8 | 10.2 | 1.143 | 1.084 | 1601 | 1459 | 1530 |
| 0.312 | 10.0 | 10.0 | 1.256 | 1.411 | 1725 | 1937 | 1831 |
| 0.625 | 9.5 | 9.4 | 2.154 | 2.049 | 3113 | 2993 | 3053 |
| 70 °C |  |  |  |  |  |  |  |
| 0 | 9.8 | 10.2 | 2.410 | 2.607 | 3377 | 3509 | 3443 |
| 0.156 | 9.5 | 10.2 | 2.415 | 2.759 | 3490 | 3714 | 3602 |
| 0.312 | 9.8 | 9.7 | 2.925 | 3.107 | 4098 | 4398 | 4248 |
| 0.625 | 9.5 | 9.9 | 2.604 | 2.615 | 3764 | 3627 | 3695 |
| 80 °C |  |  |  |  |  |  |  |
| 0 | 9.7 | 10.2 | 2.337 | 2.457 | 3308 | 3307 | 3308 |
| 0.156 | 9.9 | 10.1 | 1.955 | 1.804 | 2711 | 2452 | 2582 |
| 0.312 | 9.5 | 9.7 | 1.932 | 1.985 | 2792 | 2810 | 2801 |
| 0.625 | 9.7 | 10.3 | 2.053 | 2.229 | 2906 | 2971 | 2939 |
| 90 °C |  |  |  |  |  |  |  |
| 0 | 9.5 | 9.9 | 2.064 | 2.190 | 2983 | 2037 | 3010 |
| 0.156 | 9.5 | 10.0 | 1.877 | 1.733 | 2713 | 2380 | 2546 |
| 0.312 | 10.1 | 9.5 | 1.825 | 1.668 | 2481 | 2410 | 2446 |
| 0.625 | 9.7 | 10.0 | 1.736 | 1.689 | 2457 | 2319 | 2388 |

Table S3.4. Polymer melt and crystallisation enthalpies for the polyethylenes/ poly(ethylene-co-1-hexene) produced between 30 and 90 °C.

| Temperature (°C) | Volume 1-hexene added (mL) |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | 0 |  | 0.156 |  | 0.312 |  | 0.625 |  |
|  | ΔHm | ΔHc | ΔHm | ΔHc | ΔHm | ΔHc | ΔHm | ΔHc |
| 30 | 111 | 109 | 80 | 79 | 70 | 74 | 70 | 56 |
| 40 | 111 | 105 | 92 | 86 | 89 | 79 | 62 | 56 |
| 50 | 133 | 137 | 84 | 87 | 73 | 72 | 67 | 60 |
| 60 | 136 | 134 | 88 | 89 | 77 | 73 | 67 | 67 |
| 70 | 157 | 156 | 106 | 106 | 109 | 103 | 68 | 85 |
| 80 | 164 | 164 | 93 | 97 | 82 | 75 | 43 | 48 |

Note: ΔHm and ΔHc correspond to melt enthalpy and crystallisation enthalpy respectively. Values given as J g−1.

Table S3.5. Polymer melt and crystallisation temperatures for the polyethylenes/poly(ethylene-co-1-hexene) produced between 30 and 90 °C.

| Temperature (°C) | Volume 1-hexene added (mL) |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | 0 |  | 0.156 |  | 0.312 |  | 0.625 |  |
|  | Tm | Tc | Tm | Tc | Tm | Tc | Tm | Tc |
| 30 | 134.8 | 117.8 | 126.1 | 114.5 | 122.6 | 111.5 | 113.9 | 103.9 |
| 40 | 134.7 | 118.3 | 124.5 | 113.4 | 119.4 | 109.9 | 112.5 | 100.2 |
| 50 | 135.9 | 117.7 | 124.7 | 112.8 | 119.7 | 108.4 | 114.2 | 100.4 |
| 60 | 136.1 | 117.5 | 123.0 | 112.1 | 116.1 | 106.8 | 115.4 | 102.0 |
| 70 | 137.7 | 116.3 | 125.3 | 111.4 | 121.9 | 110.6 | 122.3 | 108.1 |
| 80 | 135.5 | 118.3 | 122.9 | 111.6 | 119.0 | 107.0 | 121.7 | 108.1 |

Tm and Tc in °C; DSC run for 3 cycles between 25 and 250 °C; Tm taken on third heating cycle and Tc from first cooling cycle.

Table S3.6. Polymerisation activities, mass of catalyst used, and mass of polymer produced. (Co)polymerisation conditions: 10 mg catalyst, 2 bar ethylene, 0, 0.156, 0.312 or 0.625 mL 1-hexene, 50 mL hexane, 150 mg TiBA, 70 °C and 30 minutes.

| Volume of 1-hexene (mL) | Mass Catalyst (mg) |  | Mass Polymer (g) |  | Activity (kgPE/molTi/h/bar) |  | Average Activity (kgPE/molTi/h/bar) |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | A | B | A | B | A | B |  |
| sMAO-Me2SB(tBuN,I*)TiCl2 |  |  |  |  |  |  |  |
| 0 | 9.8 | 10.2 | 2.410 | 2.607 | 3377 | 3509 | 3443 |
| 0.156 | 9.5 | 10.2 | 2.415 | 2.759 | 3490 | 3714 | 3602 |
| 0.312 | 9.8 | 9.7 | 2.925 | 3.107 | 4098 | 4398 | 4248 |
| 0.625 | 9.5 | 9.9 | 2.604 | 2.615 | 3764 | 3627 | 3695 |
| sMAO-Me2SB(tBuN,3-EtI*)TiCl2 |  |  |  |  |  |  |  |
| 0 | 9.6 | 9.5 | 2.534 | 2.877 | 3614 | 4146 | 3880 |
| 0.156 | 9.9 | 9.7 | 1.805 | 1.661 | 2496 | 2344 | 2420 |
| 0.312 | 9.5 | 9.8 | 1.627 | 1.655 | 2345 | 2312 | 2328 |
| 0.625 | 9.5 | 10.2 | 1.944 | 2.309 | 2801 | 3099 | 2950 |
| sMAO-Me,PrSB(tBuN,I*)TiCl2 |  |  |  |  |  |  |  |
| 0 | 10.0 | 10.1 | 2.939 | 3.100 | 4056 | 4236 | 4146 |
| 0.156 | 10.1 | 10.2 | 2.030 | 1.957 | 2774 | 2648 | 2711 |
| 0.312 | 10.3 | 10.3 | 2.137 | 2.063 | 2863 | 2764 | 2814 |
| 0.625 | 9.7 | 10.1 | 2.300 | 2.397 | 3272 | 3275 | 3274 |
| sMAO-Me2SB(tBuN,I*)Ti(CH2Ph)2 |  |  |  |  |  |  |  |
| 0 | 9.7 | 10.0 | 3.004 | 3.230 | 4285 | 4469 | 4377 |
| 0.156 | 9.7 | 10.4 | 1.856 | 1.970 | 2647 | 2621 | 2634 |
| 0.312 | 9.8 | 9.8 | 1.684 | 1.772 | 2378 | 2502 | 2440 |
| 0.625 | 9.9 | 9.5 | 2.037 | 1.824 | 2847 | 2657 | 2751 |
| sMAO-Me2SB(tBuN,Cp*)TiCl2 |  |  |  |  |  |  |  |
| 0 | 10.0 | 9.6 | 1.658 | 1.525 | 2273 | 2178 | 2226 |
| 0.156 | 9.9 | 9.9 | 1.382 | 1.291 | 1914 | 1788 | 1851 |
| 0.312 | 10.0 | 9.9 | 1.559 | 1.630 | 2137 | 2257 | 2197 |
| 0.625 | 9.7 | 10.2 | 1.179 | 1.402 | 1666 | 1884 | 1775 |

Table S3.7. Polymer melt and crystallisation temperatures for the polyethylenes/poly(ethylene-co-1-hexene) produced for the catalysts (A) sMAO-Me2SB(tBuN,I*)TiCl2, (B) sMAO-Me2SB(tBuN,3-EtI*)TiCl2, (C) sMAO-Me,PrSB(tBuN,I*)TiCl2, (D) sMAO-Me2SB(tBuN,I*)Ti(CH2Ph)2, and (E) sMAO-Me2SB(tBuN,Cp*)TiCl2. (Co)polymerisation conditions: 10 mg catalyst, 2 bar ethylene, 0, 0.156, 0.312 or 0.625 mL 1-hexene, 50 mL hexane, 150 mg TiBA and 30 minutes.

| Complex | Volume 1-hexene added (mL) |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | 0 |  | 0.156 |  | 0.312 |  | 0.625 |  |
|  | Tm | Tc | Tm | Tc | Tm | Tc | Tm | Tc |
| A | 137.7 | 116.3 | 125.3 | 111.4 | 121.9 | 110.6 | 122.3 | 108.1 |
| B | 132.7 | 119.1 | 121.7 | 111.07 | 117.2 | 106.6 | 113.8 | 98.5 |
| C | 133.2 | 119.4 | 122.8 | 110.9 | 117.3 | 107.4 | 113.8 | 101.0 |
| D | 133.5 | 118.8 | 122.3 | 112.2 | 117.0 | 106.1 | 114.3 | 102.2 |
| E | 133.7 | 118.2 | 120.0 | 109.9 | 116.9 | 104.9 | 107.0 | 94.4 |

Tm and Tc in °C; DSC run for 3 cycles between 25 and 250 °C; Tm taken on third heating cycle and Tc from first cooling cycle.

Table S3.8. Polymer melt and crystallisation enthalpies for the polyethylenes/ poly(ethylene-co-1-hexene) produced for the catalysts (A) sMAO-Me2SB(tBuN,I*)TiCl2, (B) sMAO-Me2SB(tBuN,3-EtI*)TiCl2, (C) sMAO-Me,PrSB(tBuN,I*)TiCl2, (D) sMAO-Me2SB(tBuN,I*)Ti(CH2Ph)2, and (E) sMAO-Me2SB(tBuN,Cp*)TiCl2. (Co)polymerisation conditions: 10 mg catalyst, 2 bar ethylene, 0, 0.156, 0.312 or 0.625 mL 1-hexene, 50 mL hexane, 150 mg TiBA and 30 minutes.

| Complex | Volume 1-hexene added (mL) |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | 0 |  | 0.156 |  | 0.312 |  | 0.625 |  |
|  | ΔHm | ΔHc | ΔHm | ΔHc | ΔHm | ΔHc | ΔHm | ΔHc |
| A | 157 | 156 | 106 | 106 | 109 | 103 | 68 | 85 |
| B | 145 | 145 | 99 | 95 | 83 | 83 | 60 | 56 |
| C | 129 | 130 | 89 | 82 | 79 | 76 | 60 | 62 |
| D | 153 | 142 | 94 | 87 | 56 | 55 | 70 | 62 |
| E | 159 | 150 | 98 | 96 | 78 | 77 | 48 | 50 |

Note: ΔHm and ΔHc correspond to melt enthalpy and crystallisation enthalpy respectively. Values given as J g−1.

Table S3.9. Polymerisation activities, mass of catalyst used, and mass of polymer produced. (Co)polymerisation conditions: 10 mg catalyst, 2 bar ethylene, 0, 0.156, 0.312 or 0.625 mL styrene, 50 mL hexane, 150 mg TiBA, 70 °C and 30 minutes.

| Volume of styrene (mL) | Mass Catalyst (mg) |  | Mass Polymer (g) |  | Activity (kgPE/molTi/h/bar) |  | Average Activity (kgPE/molTi/h/bar) |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | A | B | A | B | A | B |  |
| sMAO-Me2SB(tBuN,I*)TiCl2 |  |  |  |  |  |  |  |
| 0 | 9.8 | 10.2 | 2.410 | 2.607 | 3377 | 3509 | 3443 |
| 0.156 | 9.9 | 9.7 | 0.824 | 0.878 | 1143 | 1243 | 1193 |
| 0.312 | 10.4 | 9.4 | 0.918 | 0.862 | 1212 | 1259 | 1236 |
| 0.625 | 9.7 | 10.1 | 1.401 | 1.537 | 1983 | 2089 | 2036 |
| sMAO-Me2SB(tBuN,3-EtI*)TiCl2 |  |  |  |  |  |  |  |
| 0 | 9.6 | 9.5 | 2.534 | 2.877 | 3614 | 4146 | 3880 |
| 0.156 | 10.1 | 10.2 | 1.103 | 1.019 | 1495 | 1368 | 1431 |
| 0.312 | 9.8 | 10.0 | 0.980 | 0.934 | 1369 | 1279 | 1324 |
| 0.625 | 9.8 | 10.3 | 0.912 | 0.956 | 1274 | 1271 | 1272 |
| sMAO-Me,PrSB(tBuN,I*)TiCl2 |  |  |  |  |  |  |  |
| 0 | 10.0 | 10.1 | 2.939 | 3.100 | 4056 | 4236 | 4146 |
| 0.156 | 9.5 | 9.8 | 0.574 | 0.763 | 834 | 1074 | 954 |
| 0.312 | 10.4 | 9.9 | 0.652 | 0.603 | 865 | 841 | 853 |
| 0.625 | 9.5 | 10.1 | 0.472 | 0.542 | 686 | 741 | 713 |
| sMAO-Me2SB(tBuN,I*)Ti(CH2Ph)2 |  |  |  |  |  |  |  |
| 0 | 9.7 | 10.0 | 3.004 | 3.230 | 4285 | 4469 | 4377 |
| 0.156 | 9.8 | 10.1 | 0.527 | 0.691 | 744 | 947 | 845 |
| 0.312 | 10.5 | 9.5 | 0.777 | 0.542 | 1024 | 789 | 907 |
| 0.625 | 9.3 | 10.2 | 0.423 | 0.610 | 629 | 827 | 728 |
| sMAO-Me2SB(tBuN,Cp*)TiCl2 |  |  |  |  |  |  |  |
| 0 | 10.0 | 9.6 | 1.658 | 1.525 | 2273 | 2178 | 2226 |
| 0.156 | 9.7 | 9.8 | 1.660 | 1.881 | 2346 | 2632 | 2488 |
| 0.312 | 9.8 | 9.8 | 1.255 | 1.449 | 1756 | 2027 | 1891 |
| 0.625 | 10.2 | 10.2 | 1.065 | 1.035 | 1432 | 1391 | 1411 |

Table S3.10. Polymer melt and crystallisation temperatures for the polyethylenes/poly(ethylene-co-styrene) produced for the catalysts (A) sMAO-Me2SB(tBuN,I*)TiCl2, (B) sMAO-Me2SB(tBuN,3-EtI*)TiCl2, (C) sMAO-Me,PrSB(tBuN,I*)TiCl2, (D) sMAO-Me2SB(tBuN,I*)Ti(CH2Ph)2, and (E) sMAO-Me2SB(tBuN,Cp*)TiCl2. (Co)polymerisation conditions: 10 mg catalyst, 2 bar ethylene, 0, 0.156, 0.312 or 0.625 mL styrene, 50 mL hexane, 150 mg TiBA and 30 minutes.

| Complex | Volume styrene added (mL) |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | 0 |  | 0.156 |  | 0.312 |  | 0.625 |  |
|  | Tm | Tc | Tm | Tc | Tm | Tc | Tm | Tc |
| A | 137.7 | 116.3 | 119.4 | 109.7 | 115.5 | 105.5 | 97.9 | 109.7 |
| B | 132.7 | 119.1 | 120.1 | 108.9 | 114.6 | 104.2 | 107.8 | 96.4 |
| C | 133.2 | 119.4 | 121.7 | 111.6 | 119.0 | 108.9 | 113.1 | 103.2 |
| D | 133.5 | 118.8 | 119.6 | 109.0 | 115.6 | 105.3 | 110.1 | 99.9 |
| E | 133.7 | 118.2 | 115.2 | 105.2 | 108.7 | 96.7 | 98.4 | 86.7 |

Tm and Tc in °C; DSC run for 3 cycles between 25 and 250 °C; Tm taken on third heating cycle and Tc from first cooling cycle.

Table S3.11. Polymer melt and crystallisation for the polyethylenes/poly(ethylene-co-styrene) produced for the catalysts (A) sMAO-Me2SB(tBuN,I*)TiCl2, (B) sMAO-Me2SB(tBuN,3-EtI*)TiCl2, (C) sMAO-Me,PrSB(tBuN,I*)TiCl2, (D) sMAO-Me2SB(tBuN,I*)Ti(CH2Ph)2, and (E) sMAO-Me2SB(tBuN,Cp*)TiCl2. (Co)polymerisation conditions: 10 mg catalyst, 2 bar ethylene, 0, 0.156, 0.312 or 0.625 mL styrene, 50 mL hexane,150 mg TiBA and 30 minutes.

| Complex | Volume styrene added (mL) |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | 0 |  | 0.156 |  | 0.312 |  | 0.625 |  |
|  | ΔHm | ΔHc | ΔHm | ΔHc | ΔHm | ΔHc | ΔHm | ΔHc |
| A | 157 | 156 | 88 | 89 | 85 | 87 | 64 | 59 |
| B | 145 | 145 | 87 | 87 | 74 | 74 | 61 | 60 |
| C | 129 | 130 | 91 | 82 | 79 | 75 | 79 | 71 |
| D | 153 | 142 | 76 | 89 | 75 | 67 | 57 | 63 |
| E | 159 | 150 | 80 | 82 | 61 | 60 | 45 | 41 |

Note: ΔHm and ΔHc correspond to melt enthalpy and crystallisation enthalpy respectively. Values given as J g−1.

Figure S3.4. Ethylene uptake rate plots for sMAO-Me2SB(tBuN,Cp*)TiCl2. (Co)polymerisations run for 30 minutes, 10 mg catalyst, 150 mg TiBA, 2 bar of ethylene pressure and 10 mg of catalyst at 70 °C. Y-axis is a guide with percentage value providing a quantitative measure of uptake.

Figure S3.5. Ethylene uptake rate plots for sMAO-Me,PrSB(tBuN,I*)TiCl2. (Co)polymerisations run for 30 minutes, 10 mg catalyst, 150 mg TiBA, 2 bar of ethylene pressure and 10 mg of catalyst at 70 °C. Y-axis is a guide with percentage value providing a quantitative measure of uptake.

Figure S3.6. Ethylene uptake rate plots for sMAO-Me2SB(tBuN,I*)Ti(CH2Ph2). (Co)polymerisations run for 30 minutes, 10 mg catalyst, 150 mg TiBA, 2 bar of ethylene pressure and 10 mg of catalyst at 70 °C. Y-axis is a guide with percentage value providing a quantitative measure of uptake.

Figure S3.7. Ethylene uptake rate plots for sMAO-Me2SB(tBuN,3-EtI*)TiCl2. (Co)polymerisations run for 30 minutes, 10 mg catalyst, 150 mg TiBA, 2 bar of ethylene pressure and 10 mg of catalyst at 70 °C. Y-axis is a guide with percentage value providing a quantitative measure of uptake.

Figure S3.8. Ethylene uptake rate plots for sMAO-Me2SB(tBuN,I*)TiCl2 at 70 °C. (Co)polymerisations run for 30 minutes, 10 mg catalyst, 150 mg TiBA, 2 bar of ethylene pressure and 10 mg of catalyst at 70 °C. Y-axis is a guide with percentage value providing a quantitative measure of uptake.

Figure S3.9. Ethylene uptake rate plots for sMAO-Me2SB(tBuN,Cp*)TiCl2. (Co)polymerisations run for 30 minutes, 10 mg catalyst, 150 mg TiBA, 2 bar of ethylene pressure and 10 mg of catalyst at 70 °C. Y-axis is a guide with percentage value providing a quantitative measure of uptake.

Figure S3.10. Ethylene uptake rate plots for sMAO-Me,PrSB(tBuN,I*)TiCl2. (Co)polymerisations run for 30 minutes, 10 mg catalyst, 150 mg TiBA, 2 bar of ethylene pressure and 10 mg of catalyst at 70 °C. Y-axis is a guide with percentage value providing a quantitative measure of uptake.

Figure S3.11. Ethylene uptake rate plots for sMAO-Me2SB(tBuN,I*)Ti(CH2Ph2). (Co)polymerisations run for 30 minutes, 10 mg catalyst, 150 mg TiBA, 2 bar of ethylene pressure and 10 mg of catalyst at 70 °C. Y-axis is a guide with percentage value providing a quantitative measure of uptake.

Figure S3.12. Ethylene uptake rate plots for sMAO-Me2SB(tBuN,3-EtI*)TiCl2. (Co)polymerisations run for 30 minutes, 10 mg catalyst, 150 mg TiBA, 2 bar of ethylene pressure and 10 mg of catalyst at 70 °C. Y-axis is a guide with percentage value providing a quantitative measure of uptake.

Figure S3.13. GPC traces for sMAO-Me2SB(RN,I*)TiCl2. Polymerisations run for 30 minutes, 10 mg catalyst, 150 mg TiBA, 2 bar of ethylene pressure and 10 mg of catalyst at 70 °C. Y-axis is a guide with percentage value providing a quantitative measure of uptake.

Figure S3.14. GPC traces for sMAO-Me2SB(tBuN,I*)TiX2. Polymerisations run for 30 minutes, 10 mg catalyst, 150 mg TiBA, 2 bar of ethylene pressure and 10 mg of catalyst at 70 °C. Y-axis is a guide with percentage value providing a quantitative measure of uptake.

Polymer molecular weights decrease with increased polymerisation temperature (868 to 247 kDa), due to the relative rates of chain propagation and termination changing with temperature, and chain transfer reactions increasing at higher temperatures. In addition, there are greater values of polydispersities (Mw/Mn) for the less active catalysts; at 70 ºC, Mw/Mn for sMAO-Me2SB(tBuN,I*)TiCl2 is 3.9 compared with 8.4, 7.6 and 5.7 for sMAO-Me2SB(CyN,I*)TiCl2, sMAO-Me2SB(iPrN,I*)TiCl2 and sMAO-Me2SB(nBuN,I*)TiCl2 respectively.

The polymer molecular weight distributions of the polymers produced by aromatic amido complexes are in general much greater than those of the aliphatic amido complexes, with values up to 30.8. The 29Si CP-MAS ssNMR of sMAO-Me2SB(PhN,I*)TiCl2 shows multiple resonances at 6, 2, −4, −16, −98 ppm. In contrast, the 29Si CP-MAS ssNMR of sMAO-Me2SB(tBuN,I*)TiCl2 shows one resonance at −19 ppm which would imply the presence of multiple silicon species in the aromatic CGC and one in sMAO-Me2SB(tBuN,I*)TiCl2. These broad molecular weight distributions and the multiple resonances observed in the ssNMR would imply poor control of the polymerisation mechanism with aromatic CGCs, and the possibility of multiple active sites.

4. Additional X-ray crystallography data

4.1 Experimental crystallographic data

Table S4.1. Selected experimental crystallographic data.

| Complex | Me2SB(tBuN,I*)TiMe2 | Me2SB(tBuN,I*)Ti(CH2SiMe3)2 | Me2SB(tBuN,I*)Ti(Cl)CH2SiMe3 |
| --- | --- | --- | --- |
| Crystal data |  |  |  |
| Chemical formula | C23H39NSiTi | C29H55NSi3Ti | C25H44ClNSi2Ti |
| Mr | 405.54 | 549.91 | 498.14 |
| Crystal system, space group | Triclinic, P¯1 | Monoclinic, P21/c | Triclinic, P¯1 |
| Temperature (K) | 150 | 150 | 150 |
| a, b, c (Å) | 8.3867 (3), 11.9189 (3), 13.1122 (4) | 15.8252 (1), 17.4377 (2), 11.7547 (1) | 11.5116 (4), 15.3678 (4), 17.0621 (3) |
| α, β, γ (°) | 71.317 (3), 77.382 (3), 70.280 (3) | 90, 100.355 (1), 90 | 74.727 (2), 82.480 (2), 72.304 (3) |
| V (Å3) | 1159.83 (7) | 3190.94 (5) | 2769.80 (14) |
| Z | 2 | 4 | 4 |
| Radiation type | Cu Ka | Cu Ka | Cu Ka |
| µ (mm-1) | 3.65 | 3.46 | 4.41 |
| Crystal size (mm) | 0.23 × 0.17 × 0.14 | 0.32 × 0.19 × 0.17 | 0.19 × 0.14 × 0.05 |
| Data Collection |  |  |  |
| Diffractometer | SuperNova, Dual, Cu at zero, Atlas | SuperNova, Dual, Cu at zero, Atlas | SuperNova, Dual, Cu at zero, Atlas |
| Absorption correction | Gaussian CrysAlis PRO 1.171.38.41 (Rigaku Oxford Diffraction, 2015) Numerical absorption correction based on gaussian integration over a multifaceted crystal model Empirical absorption correction using spherical harmonics, implemented in SCALE3 ABSPACK scaling algorithm. | Multi-scan CrysAlis PRO 1.171.38.41 (Rigaku Oxford Diffraction, 2015) Empirical absorption correction using spherical harmonics, implemented in SCALE3 ABSPACK scaling algorithm. | Multi-scan CrysAlis PRO 1.171.39.46 (Rigaku Oxford Diffraction, 2018) Empirical absorption correction using spherical harmonics, implemented in SCALE3 ABSPACK scaling algorithm. |
| Tmin, Tmax | 0.738, 0.837 | 0.771, 1.000 | 0.870, 1.000 |
| No. of measured, independent and observed [I > 2σ(I)] reflections | 23597, 4738, 4648 | 62395, 6525, 6322 | 30077, 11479, 10137 |
| Rint | 0.019 | 0.027 | 0.032 |
| Refinement |  |  |  |
| R[F2 > 2σ(F2)], wR(F2), S | 0.029, 0.087, 1.11 | 0.027, 0.076, 1.07 | 0.036, 0.097, 1.03 |
| No. of reflections | 4738 | 6525 | 11479 |
| No. of parameters | 248 | 324 | 569 |
| No. of restraints | 0 | 0 | 0 |
| (Δ/σ)max | 0.002 | 0.002 | 0.002 |
| Δρmax, Δρmin (e Å-3) | 0.27. -0.27 | 0.27, -0.29 | 0.79, -0.34 |

Computer programs: CrysAlis PRO 1.171.38.41 (Rigaku OD, 2015), CrysAlis PRO 1.171.39.46 (Rigaku OD, 2018), SUPERFLIP-Palatinus, L.; Chapuis, G. J. Appl. Cryst. 2007, 40, 786-790., SHELXL2014/7 (Sheldrick, 2014), Burnett, M. N.; Johnson, C. K. ORTEP-III Report ORNL-6895. Oak Ridge National Laboratory, Tennessee, USA 1996.

5. References

1	J.-C. Buffet, T. A. Q. Arnold, Z. R. Turner, P. Angpanitcharoen and D. O’Hare, RSC Adv., 2015, 5, 87456–87464.

2	J. P. Fackler, Inorganic Syntheses, John Wiley & Sons, Inc., Hoboken, NJ, USA, 1982, vol. 21.

3.	J. Cosier and A. M. Glazer, J. Appl. Crystallogr., 1986, 19, 105-107.

4.	CrysAlisPRO, Oxford Diffraction /Agilent Technologies UK Ltd, Yarnton, England.

5.	A. Altomare, G. Cascarano, C. Giacovazzo and A. Guagliardi, J. Appl. Crystallogr., 1993, 26, 343-350.

6.	L. Palatinus and G. Chapuis, J. Appl. Crystallogr., 2007, 40, 786-790.

7.	L. Farrugia, J. Appl. Crystallogr., 1999, 32, 837-838.