## Slide 1: 2020-08-04_1596552220_tBP_concentration_optimization
Tuesday August 04 2020 zhous

## Slide 2
label | sub | HTM | perovskite | ETM | metal
0028C9 | FTO | Spiro-OMeTAD | FACsPbIBr | SnO2 | Au
002A82 | FTO | Spiro-OMeTAD | FACsPbIBr | SnO2 | Au
002A86 | FTO | Spiro-OMeTAD | FACsPbIBr | SnO2 | Au
002B6E | FTO | Spiro-OMeTAD | FACsPbIBr | SnO2 | Au
002B70 | FTO | Spiro-OMeTAD | FACsPbIBr | SnO2 | Au
002B72 | FTO | Spiro-OMeTAD | FACsPbIBr | SnO2 | Au
002B73 | FTO | Spiro-OMeTAD | FACsPbIBr | SnO2 | Au
002B74 | FTO | Spiro-OMeTAD | FACsPbIBr | SnO2 | Au
002B75 | FTO | Spiro-OMeTAD | FACsPbIBr | SnO2 | Au
002B76 | FTO | Spiro-OMeTAD | FACsPbIBr | SnO2 | Au
002B77 | FTO | Spiro-OMeTAD | FACsPbIBr | SnO2 | Au
002B78 | FTO | Spiro-OMeTAD | FACsPbIBr | SnO2 | Au
002B79 | FTO | Spiro-OMeTAD | FACsPbIBr | SnO2 | Au
002B7A | FTO | Spiro-OMeTAD | FACsPbIBr | SnO2 | Au
002B7B | FTO | Spiro-OMeTAD | FACsPbIBr | SnO2 | Au
002B7C | FTO | Spiro-OMeTAD | FACsPbIBr | SnO2 | Au
002B7D | FTO | Spiro-OMeTAD | FACsPbIBr | SnO2 | Au
002B7E | FTO | Spiro-OMeTAD | FACsPbIBr | SnO2 | Au
002B7F | FTO | Spiro-OMeTAD | FACsPbIBr | SnO2 | Au
002B80 | FTO | Spiro-OMeTAD | FACsPbIBr | SnO2 | Au
002B81 | FTO | Spiro-OMeTAD | FACsPbIBr | SnO2 | Au

## Slide 3: Measured illumination spectra

## Slide 4: Steady-state Parameters by label, page 0

## Slide 5: Steady-state Parameters by label, page 1

## Slide 6: J-V Parameters by label, page 0

## Slide 7: J-V Parameters by label, page 1

## Slide 8: concentration Steady-state Parameters by value, page 0

## Slide 9: concentration Steady-state Parameters by value, page 1

## Slide 10: concentration J-V Parameters by value, page 0

## Slide 11: concentration J-V Parameters by value, page 1

## Slide 12: Yields, page 0

## Slide 13: Steady-state power output, page 0

## Slide 14: Steady-state power output, page 1

## Slide 15: Steady-state power output, page 2

## Slide 16: Steady-state power output, page 3

## Slide 17: Steady-state power output, page 4

## Slide 18: Steady-state power output, page 5

## Slide 19: Steady-state power output, page 6

## Slide 20: Steady-state power output, page 7

## Slide 21: Steady-state power output, page 8

## Slide 22: Steady-state power output, page 9

## Slide 23: Steady-state power output, page 10

## Slide 24: Steady-state power output, page 11

## Slide 25: Steady-state power output, page 12

## Slide 26: Steady-state power output, page 13

## Slide 27: Steady-state power output, page 14

## Slide 28: Steady-state power output, page 15

## Slide 29: Steady-state power output, page 16

## Slide 30: Steady-state power output, page 17

## Slide 31: Steady-state power output, page 18

## Slide 32: Steady-state power output, page 19

## Slide 33: Steady-state power output, page 20

## Slide 34: Steady-state power output, page 21

## Slide 35: Steady-state power output, page 22

## Slide 36: Steady-state power output, page 23

## Slide 37: Steady-state power output, page 24

## Slide 38: Steady-state power output, page 25

## Slide 39: Steady-state power output, page 26

## Slide 40: Steady-state power output, page 27

## Slide 41: Steady-state power output, page 28

## Slide 42: Steady-state Jsc, page 0

## Slide 43: Steady-state Jsc, page 1

## Slide 44: Steady-state Jsc, page 2

## Slide 45: Steady-state Jsc, page 3

## Slide 46: Steady-state Jsc, page 4

## Slide 47: Steady-state Jsc, page 5

## Slide 48: Steady-state Jsc, page 6

## Slide 49: Steady-state Jsc, page 7

## Slide 50: Steady-state Jsc, page 8

## Slide 51: Steady-state Jsc, page 9

## Slide 52: Steady-state Jsc, page 10

## Slide 53: Steady-state Jsc, page 11

## Slide 54: Steady-state Jsc, page 12

## Slide 55: Steady-state Jsc, page 13

## Slide 56: Steady-state Jsc, page 14

## Slide 57: Steady-state Jsc, page 15

## Slide 58: Steady-state Jsc, page 16

## Slide 59: Steady-state Jsc, page 17

## Slide 60: Steady-state Jsc, page 18

## Slide 61: Steady-state Jsc, page 19

## Slide 62: Steady-state Jsc, page 20

## Slide 63: Steady-state Jsc, page 21

## Slide 64: Steady-state Jsc, page 22

## Slide 65: Steady-state Jsc, page 23

## Slide 66: Steady-state Jsc, page 24

## Slide 67: Steady-state Jsc, page 25

## Slide 68: Steady-state Jsc, page 26

## Slide 69: Steady-state Jsc, page 27

## Slide 70: Steady-state Voc, page 0

## Slide 71: Steady-state Voc, page 1

## Slide 72: Steady-state Voc, page 2

## Slide 73: Steady-state Voc, page 3

## Slide 74: Steady-state Voc, page 4

## Slide 75: Steady-state Voc, page 5

## Slide 76: Steady-state Voc, page 6

## Slide 77: Steady-state Voc, page 7

## Slide 78: Steady-state Voc, page 8

## Slide 79: Steady-state Voc, page 9

## Slide 80: Steady-state Voc, page 10

## Slide 81: Steady-state Voc, page 11

## Slide 82: Steady-state Voc, page 12

## Slide 83: Steady-state Voc, page 13

## Slide 84: Steady-state Voc, page 14

## Slide 85: Steady-state Voc, page 15

## Slide 86: Steady-state Voc, page 16

## Slide 87: Steady-state Voc, page 17

## Slide 88: Steady-state Voc, page 18

## Slide 89: Steady-state Voc, page 19

## Slide 90: Steady-state Voc, page 20

## Slide 91: Steady-state Voc, page 21

## Slide 92: Steady-state Voc, page 22

## Slide 93: Steady-state Voc, page 23

## Slide 94: Steady-state Voc, page 24

## Slide 95: Steady-state Voc, page 25

## Slide 96: Steady-state Voc, page 26

## Slide 97: Steady-state Voc, page 27

## Slide 98: Steady-state Voc, page 28

## Slide 99: Best JV scans of every working pixel, page 0

## Slide 100: Best JV scans of every working pixel, page 1

## Slide 101: Best JV scans of every working pixel, page 2

## Slide 102: Best JV scans of every working pixel, page 3

## Slide 103: Best JV scans of every working pixel, page 4

## Slide 104: Best JV scans of every working pixel, page 5

## Slide 105: Best pixel JVs, page 0

## Slide 106: Best pixel JVs, page 1

## Slide 107: Best pixel JVs, page 2

## Slide 108: Best pixel JVs, page 3

## Slide 109: All JV scans, page 0

## Slide 110: All JV scans, page 1

## Slide 111: All JV scans, page 2

## Slide 112: All JV scans, page 3

## Slide 113: All JV scans, page 4

## Slide 114: All JV scans, page 5

## Slide 115: All JV scans, page 6

## Slide 116: All JV scans, page 7

## Slide 117: All JV scans, page 8

## Slide 118: All JV scans, page 9

## Slide 119: All JV scans, page 10

## Slide 120: All JV scans, page 11

## Slide 121: All JV scans, page 12

## Slide 122: All JV scans, page 13

## Slide 123: All JV scans, page 14

## Slide 124: All JV scans, page 15

## Slide 125: All JV scans, page 16

## Slide 126: All JV scans, page 17

## Slide 127: All JV scans, page 18

## Slide 128: All JV scans, page 19

## Slide 129: All JV scans, page 20

## Slide 130: All JV scans, page 21

## Slide 131: All JV scans, page 22

## Slide 132: All JV scans, page 23

## Slide 133: All JV scans, page 24

## Slide 134: All JV scans, page 25

## Slide 135: All JV scans, page 26

## Slide 136: All JV scans, page 27

## Slide 137: All JV scans, page 28