## Slide 1: AFM
Sample ID | Description (Glass/ITO/PEDOT:PSS/ …)
B | Neat 1.2M-Perovskite
D | Neat 1.8M-Perovskite
E | 1.8M-Perovskite / Al2O3 NPs
G | 1.8M-Perovskite / PCBM
J | 1.8M-Perovskite / Al2O3 NPs / PCBM
Sample details

## Slide 2: AFM
Sample B: Neat 1.2M-PVSK
500 mm
Optical image of ROI
Est. RMS surface roughness (Sq) ~ 27.5 nm

## Slide 3: AFM
Sample D: Neat 1.8M-PVSK
500 mm
Optical image of ROI
Est. RMS surface roughness (Sq) ~ 42.8 nm

## Slide 4: AFM
Sample E: 1.8M-PVSK / Al2O3 NPs
Est. RMS surface roughness (Sq) ~ 37.2 nm

## Slide 5: AFM
Sample G: 1.8M-PVSK / PCBM
500 mm
Optical image of ROI
Est. RMS surface roughness (Sq) ~ 16.8 nm

## Slide 6: AFM
Sample J: 1.8M-PVSK / Al2O3 NPs / PCBM
500 mm
Optical image of ROI
Est. RMS surface roughness (Sq) ~ 32.0 nm

## Slide 7: AFM
Surface roughness estimates
Sample | Scan size (mm) | Scan area (mm2) | Roughness (nm) |  | 
Sample | Scan size (um) | Scan area (um2) | Avg | Sq | Sa
B - 1.2M Perovskite | 5 | 25 | 94.3 | 27.46 | 21.81
D - 1.8M Perovskite | 5 | 25 | 162.6 | 42.8 | 33.2
E - 1.8M PVSK / Al2O3-NP | 5 | 25 | 177.1 | 37.22 | 29.39
 | 2.5 | 6.25 | 123.1 | 29.44 | 23.56
 | 2.5 | 6.25 | 114.6 | 28.72 | 23
G - 1.8M PVSK / PCBM | 5 | 25 | 51.6 | 16.8 | 12.98
J - 1.8M PVSK / Al2O3 / PCBM | 5 | 25 | 101.6 | 31.99 | 25.16
 | 2.5 | 6.25 | 82.1 | 22.95 | 18.4

## Slide 8: AFM