Spectrum processing :

Peaks possibly omitted : 0.938, 4.529, 6.885, 8.051 keV

Quantitation method : Cliff Lorimer thin ratio section.

Processing option : All elements analyzed (Normalised)

Number of iterations = 2

Standardless

| Element | Weight% | Atomic% |  |
| --- | --- | --- | --- |
| S K | 1.36 | 7.28 |  |
| Cd L | 16.03 | 24.42 |  |
| Pb L | 82.61 | 68.29 |  |
| Totals | 100.00 |  |  |

26/11/2013 15:01:43

Project 1

Comment: