I'm quite certain its PbS rock salt, CdS- zinc blende. (not wurtzite)

Overall size: Core diameter (PbS core): 2.4nm, Total diameter: 2.8nm

some of this i used formulae to calculate Like

PbS

lattice constant, 5.9362 A   Space grp: Fm3m

bulk modulus, 52.11GPa

young modulus,  76.9GpA

shear modulus,  22.07 MPa

poisson ratio   0.23

| Young's Modulus E: | 70.20 GPa |
| --- | --- |
| Poisson's Ratio : | 0.28 |
| Shear Modulus G: | 27.42 GPa |
| Bulk Modulus K: | 53.18 GPa |

1

CdS

lattice constant, 5.832 A       F-43m

bulk modulus, 69.44 GPa

young modulus, 61.52 GPa

shear modulus, 22.75 GPa

poisson ratio 0.3523

Young's Modulus E:

Poisson's Ratio :

Shear Modulus G:

Bulk Modulus K:

CdS 77.9

52.7 24.1

B=61.1

G=

Material

Temperature

(K) C11 C12 C44 Ref.

Ge 298 1.2835 0.4823 0.6666 20

HgTe 290 0.548 0.381 0.204 36

InAs 293 0.8329 0.4526 0.3959 23

InP RT 1.0220 0.5760 0.4600 24

InSb 298 0.6720 0.3670 0.3020 22

KBr 298 0.3468 0.0580 0.0507 11

KCl 298 0.4069 0.0711 0.0631 11

KCN RT 0.1940 0.1180 0.0150 32

KF 295 0.6490 0.1520 0.1232 33

KI 300 0.2710 0.0450 0.0364 42

KMgF3 RT 1.32 0.396 0.485 118

KTaO3 RT 4.31 1.03 1.09 117

LiBr RT 0.3940 0.1880 0.1910 32

LiCl 295 0.4927 0.2310 0.2495 33

LiF RT 1.1397 0.4767 0.6364 34

LiI RT 0.2850 0.1400 0.1350 32

Lu3Al5O12 RT 3.39 1.14 1.13 119

MgAl2O4 298 2.9857 1.5372 1.5758 53

MgO 298 2.9708 0.9536 1.5613 20

MnO 298 2.23 1.20 0.79 35

NaBr 300 0.3970 0.1001 0.0998 33

NaBrO3 RT 0.5450 0.1910 0.1500 32

NaCl 298 0.4947 0.1288 0.1287 11

NaClO3 RT 0.4920 0.1420 0.1160 50

NaF 300 0.9700 0.2380 0.2822 51

NaI 300 0.3007 0.0912 0.0733 52

NH4Br 300 0.3414 0.0782 0.0722 3

NH4Cl 290 0.3814 0.0866 0.0903 4

Pb(NO3)2 293 0.3729 0.2765 0.1347 29

PbF2 300 0.8880 0.4720 0.2454 28

PbS RT 1.26 0.162 0.171 117