# Supplementary Information

Supplementary Figure 1: SEM images of track C5 before irradiation. The measured track width (dimension A) was 48µm.

Supplementary Figure 2: (a) Temperature versus critical current measurement for sample C5 when pristine and unirradiated. “Expected” values take from RRI database for sample Fujikura FYSC 2G HTS  (available at http://htsdb.wimbush.eu/). (b) Measured temperatures of sample C5 during its cold irradiation. Periods where the beam is being applied to the sample are shown in grey. Labels: ‘A’: during this period, the temperature control system malfunctioned; ‘#56’: temperature rise due to the long beam-on pulse.

Quench of Unirradiated versus irradiation sample C4

An additional aspect of the evolution of Jc of sample C4 during its first cold irradiation cycle is that C4 suffered from two short resistive quenches during testing; the first during testing prior to irradiation  (label A, Supplementary Figure 3) and the second after the sample had been irradiated to about 1 mdpa (labelled B, Supplementary Figure 3). The first quench resulted in a small reduction in Jc (15.2 to 14.2 MA cm-2) whilst the quench after 1 mdpa of damage resulted in an increase in Jc (9.1 to 9.9 MA cm-2).

Supplementary Figure 3: A closer look at the critical current density (Jc) evolution of sample C4 normalised to its initial value (Jc(initial)) with increasing irradiation damage from 2MeV helium ions. Bold blue arrows are included to indicate a change due to room temperature annealing. Red arrow A indicates a resistive quench of the sample before irradiation leads to a reduction in Jc. Red arrow B indicates a resistive quench of the sample after it had been further irradiated to ≈1 mdpa leads to an improvement in Jc.

Supplementary Table 1: Results from the 2 cold irradiation and room temperature annealing cycles of sample C4.

| Sample C4 | First Cold Irradiation |  |  | Second Cold Irradiation |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | Tc [K] | ΔTc [K] | Ic(40K) [A] | Tc [K] | ΔTc [K] | Ic(40K) [A] |
| Initial value | 90.5 | 0.9 | 14.1 | ≈80 | 4.1 | 3.5 |
| Total damage [mdpa] | 4.47 |  |  | 6.1 |  |  |
| Post irradiation values | 65.0 | 7.3 | 0.7 | 64.9 | 7.6 | 0.8 |
| Fast recovery period [days] | 3 |  |  | 6 |  |  |
| Values after fast recovery period | 75.3 | 4.2 | 3.0 | 69.8 | 6.0 | 1.5 |
| Slow recovery period [days] | 104 |  |  | 106 |  |  |
| Values after slow recovery period | ≈80 | 4.1 | 3.5 | 75.8 | 4.5 | 2.7 |
| Values after furnace anneal | - | - | - | 80.1 | 3.8 | 4.0 |

Model for temperature in REBCO layer due to ion beam heating

Model the REBCO layer as a thin slab of thickness, t, containing a uniform distribution of point heat sources of power per unit volume  Wm-3.

Consider the heat flux, q, through a slice of thickness dz.  At steady state

q+ αdz=q+dqdzdz

α=dqdz

By definition, the heat flux is related to the temperature gradient by equation  q=-kdTdz where k is the thermal conductivity of the material.  Therefore

α=dqdz=-kd2Tdz2

Integrating gives

T=-αz22k+az+b

where a and b are constants.

Assuming for simplicity that the surfaces z=±t2 are fixed at temperature Ts then a=0 and b=Ts+αt28k and

T-Ts=α8kt2-4z2

Temperature will be a maximum at the centre of the slab (z=0) where

Tmax-Ts=αt28k

 can be estimated from the energy deposited in the REBCO layer per ion (E), the flux of ions (J) and the film thickness (t)

α=EJt

Given that t=10-6 m, Ts=40 K, kat 40 K≈0.5 Wm-1K-1 [48] and E=4.8×105 eV from SRIM calculations), we find

Tmax-Ts=EJt8k≈10-4 K

Energy deposited in REBCO layer by ion beam per unit cell

Supplementary Table 2: Results of SRIM calculations for the average energy transferred into recoils (nuclear collisions) and ionization (electronic interactions) in the REBCO layer from 2 MeV He+ ions.

| Interaction type | Energy lost to REBCO layer (eV) per ion | Fraction of incident beam energy | Fraction of energy lost in REBCO layer |
| --- | --- | --- | --- |
| Recoils (nuclear) | En=410 | 0.02% | 0.01% |
| Ionisation (electronic) | Ee=482,170 | 24% | 99.9% |

Given that the flux of incident ions, J=6.25×1015 m-2s-1, the energy deposited into REBCO layer per unit area per second =En+EeJ≈3×1021 eV m-2s-1

This can be converted to an energy per unit volume per second of 3×1027 eV m-2s-1  by dividing by the thickness of the REBCO layer.  Since the unit cell volume is 3.82×3.89×11.68 Å3≈1.7×10-28 m-3 the energy deposited per unit cell per second of 0.5 eV s-1.