## Slide 1: FTPS Urbach Tail Measurement
Qimu Yuan
Feb 2024

## Slide 2: Measurement Summary
EQE/Urbach tail measured via FTPS for a solar cell with roughly 1.68 eV band gap;
Approximately 1 sun intensity of Xe lamp illumination on the sample was calibrated via the reference Si cell;
A low pass 715 nm filter was used so that the absorption band edge could be measured to a higher sensitivity;
Sample (Cell BF37 pixel 2) was aged in air and under illumination for approximately 160 min;
To obtain EQE, the measured spectra were corrected based on the spectra of a calibrated silicon reference cell from Newport;
For fitting the Urbach tail, a single exponential in the form of
was applied in the region near the band edge for extracting Urbach energy (Eu).

## Slide 3: Urbach Tail from Xenon Lamp Aging
Semi-log plot showing external quantum efficiency at the absorption onset. The measured solar cell was illuminated by a Xenon lamp source which simulated full-spectrum AM1.5 irradiance, and held at open-circuit condition in air at room temperature for up to 160 minutes.

## Slide 4: Urbach Tail Fitting
Semi-log plots of external quantum efficiency (EQE) at the absorption onset of the same cell from starting the Xe lamp illumination to after 160 minutes of continuous illumination in air. Fitted Urbach tails from a section of EQE below the band edge indicate minimum change in the Urbach energy from irradiation.

## Slide 5: Summary
Key findings:
The measured solar cell exhibits good stability under 1 sun irradiance from the Xenon lamp in air with minimal differences observed from the Urbach tail, indicating no changes in the absorption onset or potential presence of halide segregation;
Extracted Urbach energy values from fittings suggest no time-dependent variation in the electronic disorder of this solar cell;
Additional points:
The actual band edge of this solar cell is likely to be a bit lower than the expected 1.68 eV;