## Slide 1: FTPS Urbach Tail Measurement for David & Xinyi
Qimu Yuan
Feb 2024

## Slide 2: Measurement and Technqiue Summary
EQE/Urbach tail measured via FTPS for both solar cells made from solution-processing and vapour-deposition with a roughly 1.68 eV bandgap;
Approximately 1 sun intensity of Xe lamp was illuminated on both samples, this was calibrated via measuring the reference Si cell under the solar simulator and measuring the intensity;
A long pass RG 715 nm filter was used so that the absorption band edge could be measured to a higher sensitivity, for 2nd measurement on the solution-processed device, additional long pass RG780 filter was used to further improve sub-bandgap signal sensitivity;
Both samples (BF37 Pixel 2 & D216 Pixel 6) were aged in air and under Xe illumination for approximately 160 min;
To obtain EQE, the measured spectra were corrected based on the spectra of a calibrated silicon reference cell from Newport;
For fitting the Urbach tail, a single exponential in the form of
was applied in the region near the band edge for extracting Urbach energy (Eu).

## Slide 3: Urbach Tail from Xenon Lamp Aging
Semi-log plot showing external quantum efficiency at the absorption onset. The measured solar cells were illuminated by a Xenon lamp source which simulated full-spectrum AM1.5 irradiance, and held at open-circuit condition in air at room temperature for up to 160 minutes.

## Slide 4: Urbach Tail Fitting – Vapour-deposited device
Semi-log plots of external quantum efficiency (EQE) at the absorption onset of the same vapour-deposited cell from the start of Xe lamp illumination to after 160 minutes of continuous illumination in air. Fitted Urbach tails from a section of EQE below the band edge indicate minimum change in the Urbach energy from irradiation.

## Slide 5: Urbach Tail Fitting – Solution-processed device
Semi-log plots of external quantum efficiency (EQE) at the absorption onset of the same solution-processed cell from the start of Xe lamp illumination to after 160 minutes of continuous illumination in air. Here, two measurements with different RG filters were performed. Data with energy less than 1.59 eV are from measurement with the long-pass RG780 filter. Fitted Urbach tails from a section of EQE below the band edge indicate minimum change in the Urbach energy from irradiation.

## Slide 6: Summary
Key findings:
The measured solar cells, solution-processed or vapour-deposited exhibit good stability under approximately 1 sun irradiance from the Xenon lamp in air with minimal differences observed from the Urbach tail, indicating no changes in the absorption onset or potential presence of halide segregation;
Extracted Urbach energy values from fittings suggest no time-dependent variation in the electronic disorder of this solar cell, although the Urbach energy extracted is slightly lower for solution-processed devices than for vapour-deposited devices;
Additional points:
The actual band edges of the solution-processed and vapour-deposited solar cells are different, whilst solution-processed device most likely have a bandgap around 1.68 eV, such bandgap of evaporated cell is likely to be a bit lower.