Supplemental Material

The origins of pressure-induced phase transformations during the surface texturing of silicon using femtosecond laser irradiation

Matthew J. Smith1, Meng-Ju Sher2, Benjamin Franta3, Yu-Ting Lin3, Eric Mazur2,3, Silvija Gradečak1

1. Department of Materials Science and Engineering, Massachusetts Institute of Technology, Cambridge, Massachusetts 02139, USA.

2. Department of Physics, and 3. School of Engineering and Applied Sciences, Harvard University, Cambridge, Massachusetts 02138, USA.

Figure S1. Cross-sectional bright field transmission electron microscopy (TEM) image showing the microstructure at the center of the (a) FM4 and (b) FM5 laser-irradiated spots described in the main text. Gray dashed lines indicate areas of interest presented in Figure 5 of the main text. Samples consistently show formation of sub-surface amorphous silicon only within the protruding surface peaks, and allow for estimation of the melt depth on the surface. TEM samples were prepared using focus ion beam and dark contrast comes from a protective layer of Pt deposited on the surface.