## Slide 1: 2021-05-29_1622283394_20210529_TAPTZ_ionic_passivation_WBG
Saturday May 29 2021 shenx

## Slide 2
label | sub | HTM | perovskite | ETM | metal
44DD | ITO | Me-4PACz | FACsPbIBr | C60/BCP | Ag
44DE | ITO | Me-4PACz | FACsPbIBr | C60/BCP | Ag
44E0 | ITO | tBu-4PACz | FACsPbIBr | C60/BCP | Ag
44E1 | ITO | tBu-4PACz | FACsPbIBr | C60/BCP | Ag
44E2 | ITO | PAPTZ | FACsPbIBr | C60/BCP | Ag
44E3 | ITO | PAPTZ | FACsPbIBr | C60/BCP | Ag
44E4 | ITO | Me-4PACz | FACsPbIBr | C60/BCP | Ag
44E5 | ITO | Me-4PACz | FACsPbIBr | C60/BCP | Ag
44E6 | ITO | Me-4PACz | FACsPbIBr | C60/BCP | Ag
44E7 | ITO | Me-4PACz | FACsPbIBr | C60/BCP | Ag
44E8 | ITO | Me-4PACz | FACsPbIBr | C60/BCP | Ag

## Slide 3: Measured illumination spectra

## Slide 4: Steady-state Parameters by label, page 0

## Slide 5: Steady-state Parameters by label, page 1

## Slide 6: J-V Parameters by label, page 0

## Slide 7: J-V Parameters by label, page 1

## Slide 8: various Steady-state Parameters by value, page 0

## Slide 9: various Steady-state Parameters by value, page 1

## Slide 10: various J-V Parameters by value, page 0

## Slide 11: various J-V Parameters by value, page 1

## Slide 12: Yields, page 0

## Slide 13: Steady-state power output, page 0

## Slide 14: Steady-state power output, page 1

## Slide 15: Steady-state power output, page 2

## Slide 16: Steady-state power output, page 3

## Slide 17: Steady-state power output, page 4

## Slide 18: Steady-state power output, page 5

## Slide 19: Steady-state power output, page 6

## Slide 20: Steady-state power output, page 7

## Slide 21: Steady-state power output, page 8

## Slide 22: Steady-state power output, page 9

## Slide 23: Steady-state power output, page 10

## Slide 24: Steady-state power output, page 11

## Slide 25: Steady-state power output, page 12

## Slide 26: Steady-state Jsc, page 0

## Slide 27: Steady-state Jsc, page 1

## Slide 28: Steady-state Jsc, page 2

## Slide 29: Steady-state Jsc, page 3

## Slide 30: Steady-state Jsc, page 4

## Slide 31: Steady-state Jsc, page 5

## Slide 32: Steady-state Jsc, page 6

## Slide 33: Steady-state Jsc, page 7

## Slide 34: Steady-state Jsc, page 8

## Slide 35: Steady-state Jsc, page 9

## Slide 36: Steady-state Jsc, page 10

## Slide 37: Steady-state Jsc, page 11

## Slide 38: Steady-state Voc, page 0

## Slide 39: Steady-state Voc, page 1

## Slide 40: Steady-state Voc, page 2

## Slide 41: Steady-state Voc, page 3

## Slide 42: Steady-state Voc, page 4

## Slide 43: Steady-state Voc, page 5

## Slide 44: Steady-state Voc, page 6

## Slide 45: Steady-state Voc, page 7

## Slide 46: Steady-state Voc, page 8

## Slide 47: Steady-state Voc, page 9

## Slide 48: Steady-state Voc, page 10

## Slide 49: Steady-state Voc, page 11

## Slide 50: Steady-state Voc, page 12

## Slide 51: Best JV scans of every working pixel, page 0

## Slide 52: Best JV scans of every working pixel, page 1

## Slide 53: Best JV scans of every working pixel, page 2

## Slide 54: Best pixel JVs, page 0

## Slide 55: Best pixel JVs, page 1

## Slide 56: All JV scans, page 0

## Slide 57: All JV scans, page 1

## Slide 58: All JV scans, page 2

## Slide 59: All JV scans, page 3

## Slide 60: All JV scans, page 4

## Slide 61: All JV scans, page 5

## Slide 62: All JV scans, page 6

## Slide 63: All JV scans, page 7

## Slide 64: All JV scans, page 8

## Slide 65: All JV scans, page 9

## Slide 66: All JV scans, page 10