## Slide 1
(a)
(c)
(d)
(b)
Notes: Supplementary Figure 1. (a) ηmpp, (b) steady-state VOC, (c) steady-state JSC and (d) quasi-FF of FA0.83Cs0.17Pb(I0.6Br0.4)3 PSCs employing PTAA, MeO-2PACz, 2PACz and Me-4PACz respectively as the hole transport layer. These devices were fabricated in a single experimental batch. Any pixel with ηmpp ≤ 75% ηmpp of the champion device are cut off from the figure.

## Slide 2
Notes: Supplementary Figure 2. J-V scan of the champion cells of FA0.83Cs0.17Pb(I0.6Br0.4)3 on PTAA, MeO-2PACz, 2PACz or Me-4PACz. Solid curve: reverse scan, dashed curve: forward scan. All performance metrics are given in Supplementary table 1.

## Slide 3
Devices | Scan Direction | VOC (V) | JSC/Integrated JSC (mA cm-2) | FF | PCE (%)
PTAA | Reverse | 1.09 | 16.38 | 0.716 | 12.71
 | Forward | 1.08 | 16.27 | 0.688 | 12.07
 | Steady-State | 1.08 | 15.80/16.07 | 0.745 | 12.74
MeO-2PACz | Reverse | 1.15 | 17.18 | 0.759 | 14.92
 | Forward | 1.13 | 17.12 | 0.737 | 14.24
 | Steady-State | 1.13 | 15.59/16.68 | 0.793 | 14.00
2PACz | Reverse | 1.22 | 16.92 | 0.744 | 15.31
 | Forward | 1.20 | 16.83 | 0.725 | 14.59
 | Steady-State | 1.21 | 16.77/16.96 | 0.753 | 15.24
Me-4PACz | Reverse | 1.22 | 17.28 | 0.760 | 16.08
 | Forward | 1.20 | 17.24 | 0.756 | 15.73
 | Steady-State | 1.22 | 17.14/17.33 | 0.765 | 15.95
Notes: Supplementary Table 1. PV metrics of the champion cells of FA0.83Cs0.17Pb(I0.6Br0.4)3 on PTAA, MeO-2PACz, 2PACz or Me-4PACz extracted from J-V scans in Supplementary Figure 2. *Integrated JSC extracted from EQE measurements in Supplementary Figure 3.

## Slide 4
Notes: Supplementary Figure 3. External quantum efficiency (EQE) spectra (right axis) and the corresponding integrated current density (integration of the product of EQE and AM 1.5G spectrum) (left axis) of the FA0.83Cs0.17Pb(I0.6Br0.4)3 perovskite solar cells based on PTAA, MeO-2PACz, 2PACz and Me-4PACz.

## Slide 5
(c)
(d)
(a)
(b)
Notes: Supplementary Figure 4. PV parameters of FA0.83Cs0.17Pb(I0.6Br0.4)3 PSCs based on Me-4PACz with no MACl additives (control) or 15 mol% MACl additives annealed at different conditions: (a) ηmpp, (b) steady-state VOC, (c) steady-state JSC, (d) quasi-FF. The devices were either annealed in the glovebox (N2 atmosphere, ‘in’) or transferred out of the glovebox immediately after deposition and annealed at ambient conditions (RH = 30%, ‘out’). The annealing temperature and time were selected between 30 min at 100 °C (‘100C’) or 10 min at 150 °C (‘150C’). All devices (59 cells) were fabricated in two batches of experiments.

## Slide 6
(c)
(d)
(a)
(b)
Notes: Supplementary Figure 5. PV parameters of FA0.83Cs0.17Pb(I0.6Br0.4)3 PSCs based on Me-4PACz with 15 mol% MACl additives annealed at various conditions: (a) ηmpp, (b) steady-state VOC, (c) steady-state JSC, (d) quasi-FF. The devices were deposited in the glovebox and transferred out to anneal at 150 °C for 10 min in a dry box purged with N2 (< 1% RH, ‘N2’); or a dry box purged with compressed air (< 1% RH, ‘Dry Air (< 1% RH)’); or at ambient conditions (30% RH, ‘Ambient (30% RH)’). All devices (23 cells) were fabricated in one experimental batch.

## Slide 7
Notes: Supplementary Figure 6. Steady-state PL spectra of 15 mol% MACl additive-modified or control perovskite films on quartz under continuous illumination equivalent to 29 suns. Inset: normalised PL spectra.

## Slide 8
Notes: Supplementary Figure 7: X-ray diffraction (XRD) patterns of FA0.83Cs0.17Pb(I0.6Br0.4)3 as a function of MACl additive concentration. “Control” contains 0 mol% MACl additive and is annealed at 100 °C in a N2 glovebox, whereas perovskites fabricated with MACl additive are annealed at 150 °C in air with ~30% RH. “0 mol% MACl” refers to a film without MACl additive but is annealed at 150 °C in air with ~30% RH.

## Slide 9
(c)
(d)
(a)
(b)
Notes: Supplementary Figure 8. PV parameters of FA0.83Cs0.17Pb(I0.6Br0.4)3 PSCs based on Me-4PACz with different excess molar ratio of MACl additives (0 - 45 mol%): (a) ηmpp, (b) steady-state VOC, (c) steady-state JSC, (d) quasi-FF. These devices (101 cells in total) were fabricated in 3 batches of experiments.

## Slide 10
Notes: Supplementary Figure 9. Short-range mobility of 15 mol% MACl-modified and no-MACl control films, namely ‘MACl’ or ‘Control’, characterised by Optical-Pump Terahertz-Probe spectroscopy. One control sample and 2 MACl samples were measured.

## Slide 11
Control
15 mol% MACl
Control
15 mol% MACl
Notes: Supplementary Figure 10. Top-down SEM images of (a - b) control (FA0.83Cs0.17Pb(I0.6Br0.4)3) films and (c - d) 15 mol% MACl additive-modified films.

## Slide 12
Notes: Supplementary Figure 11. Tauc analyses based on transmittance and reflectance measurements taken on FA0.83Cs0.17Pb(I0.6Br0.4)3 perovskites with a range of MACl concentrations (x) with 0 ≤ x ≤ 45 mol%. “Control” contains 0 mol% MACl additive and is annealed at 100 °C in a N2 glovebox. “0 mol% MACl” refers to a film without MACl additive but is annealed at 150 °C in air with ~30% RH.

## Slide 13
Notes: Supplementary Figure 12. EQE and integrated JSC for 15 mol% MACl additive device and control device with Me-4PACz as the HTL and C60 as the ETL, namely 15 mol% MACl or Control.

## Slide 14
(a)
(b)
Notes: Supplementary Figure 13. PV bandgap extracted from the inflection point of the onset of the EQE (Supplementary Figure 12) for (a) 15 mol% MACl additive device and (b) control device with Me-4PACz as the HTL and C60 as the ETL, namely 15 mol% MACl or Control.

## Slide 15
Notes: Supplementary Figure 14. 1H Nuclear Magnetic Resonance (NMR) spectra of control (top) and 15 mol% MACl additive (bottom)-modified perovskite materials.

## Slide 16
Notes: Supplementary Figure 15. (a) Absorbance spectra of a range of FA0.83Cs0.17Pb(I0.6Br0.4)3 perovskites each with 15 mol% additive A-site halide. MA(I0.6Br0.4) represents a mixed-halide additive with 0.6:0.4 MAI:MABr stoichiometry, at 15 mol% excess with respect to MA. (FA0.83Cs0.17)Cl represents a mixed-A-site additive 0.83:0.17 with FACl:CsCl, at 15 mol% excess with respect to Cl. The region of the spectrum highlighted in the box is expanded and the absorbance spectra normalised between 650 and 725 nm to emphasise the bandgap shifts observed as a result of 15 mol% AX addition: (b) shows the influence of MAX additives, (c) shows the influence of ACl additives.

## Slide 17
Notes: Supplementary Figure 16. X-ray diffraction patterns (XRD) showing the perovskite materials obtained by employing various AX-type additives at 15 mol% excess. MA(I0.6Br0.4) represents a mixed-halide additive with 0.6:0.4 MAI:MABr stoichiometry, at 15 mol% excess with respect to MA. (FA0.83Cs0.17)Cl represents a mixed-A-site additive 0.83:0.17 with FACl:CsCl, at 15 mol% excess with respect to Cl. The region of highlighted with a box emphasises the formation of lower-dimensionality polytypes in the presence of MAI and MABr additives.

## Slide 18
(c)
(d)
(a)
(b)
Notes: Supplementary Figure 17. Statistics of (a) ηmpp, (b) steady-state VOC, (c) steady-state JSC and (d) quasi-FF values of FA0.83Cs0.17Pb(I0.6Br0.4)3 devices based on Me-4PACz with no additive (control, 6 cells), or with 15 mol% addition of MACl (17 cells), %FACl (7 cells), %CsCl (6 cells), %FA0.83Cs0.17Cl (8 cells), %MAl (10 cells), %MABr (12 cells) or %MAI0.6Br0.4 (12 cells). These cells were fabricated across two batches of experiments.

## Slide 19
Control
15 mol% MACl
15 mol% FACl
15 mol% FA0.83Cs0.17Cl
15 mol% CsCl
15 mol% MAI
15 mol% MABr
15 mol% MAI0.6Br0.4
(a)
(b)
(c)
Notes: Supplementary Figure 18. Photos of the intermediate phases of FA0.83Cs0.17Pb(I0.6Br0.4)3 with no additive (Control) or with 15 mol% MACl, FACl, CsCl, FA0.83Cs0.17Cl, MAl, MABr or MAI0.6Br0.4 taken (a) immediately after spin coating (b) 30 min stored under N2 atmosphere and (c) 60 min stored under N2 atmosphere followed by exposure to air for 5 min.

## Slide 20
Control
15 mol%
MACl
Control
15 mol%
MACl
Notes: Supplementary Figure 19. Evolution of the absorption and photoluminescence spectra of the antisolvent-quenched (a - c) control films and (b - d) with 15 mol% MACl measured under ambient conditions (25 °C, RH ~ 30% in air).

## Slide 21
Notes: Supplementary Figure 20. XRD patterns tracking the evolution of cubic perovskite (100) and (110) reflections during step-wise annealing of (a - b) 15 mol% MACl and (c - d) control perovskite films. The control film, with no MACl additive, is annealed at 100 °C in a N2 glovebox, whereas perovskites fabricated with 15 mol% MACl additive are annealed at 150 °C in air with ~30% RH.

## Slide 22
Notes: Supplementary Figure 21: X-ray diffraction (XRD) patterns showing control and 15 mol% MACl-doped antisolvent-quenched intermediate materials in the region where reflections corresponding to hexagonal ABX3 polytypes are observed. Predicted XRD patterns for hexagonal polytypes, taken from Gratia, et al.,[6] are also shown.

## Slide 23
Notes: Supplementary Figure 22. Solvent quenching of the control (FA0.83Cs0.17Pb(I0.6Br0.4)3) or 15 mol% or 24 mol% MACl additive-modified perovskite precursor solutions under N2 atmosphere by anti-solvent dripping with anisole. 320 µL of anisole is added dropwise (10 µL each time) into 100 µL of perovskite precursors. A same amount of anisole is used in our PSC device fabrications. Any changes in the solution appearance over time are recorded with a digital camera. The photos taken before antisolvent dripping; after adding 80 µL, 160 µL, 240 µL, 320 µL of anisole; stirring in glovebox after solvent quenching are shown in the graph.

## Slide 24
(a)
(b)
Notes: Supplementary Figure 23. GIWAXS patterns tracking the evolution of cubic perovskite (100) reflection during step-wise annealing of (a) control and (b) 15 mol% MACl-modified perovskite films.

## Slide 25
Notes: Supplementary Figure 24. Normalised PL spectra of intermediates formed for FA0.83Cs0.17Pb(I0.6Br0.4)3 and FA0.83Cs0.17Pb(I0.6Br0.4)3 with 15 mol% MACl additive after 1 s thermal annealing at 60 °C, denoted as ‘Control’ and ‘15 mol% MACl’.

## Slide 26
Devices | Scan Direction | VOC (V) | JSC (mA cm-2) | FF | PCE (%)
PTAA | Reverse | 1.07 | 17.28 | 0.741 | 13.75
 | Forward | 1.06 | 17.29 | 0.733 | 13.51
 | Steady-State | 1.07 | 16.46 | 0.750 | 13.26
Me-4PACz | Reverse | 1.23 | 17.38 | 0.780 | 16.61
 | Forward | 1.21 | 17.37 | 0.768 | 16.13
 | Steady-State | 1.22 | 17.27 | 0.784 | 16.52
Me-4PACz + 15 mol% MACl | Reverse | 1.25 | 17.24 | 0.799 | 17.41
 | Forward | 1.22 | 17.21 | 0.779 | 16.59
 | Steady-State | 1.25 | 17.17 | 0.782 | 17.00
Notes: Supplementary Table 2. Device performance of the optimised perovskite solar cells. PV metrics extracted from the J-V scan and maximum power point tracking of the champion cells (FA0.83Cs0.17Pb(I0.6Br0.4)3 on PTAA or Me-4PACz and FA0.83Cs0.17Pb(I0.6Br0.4)3 + 15 mol% MACl on Me-4PACz).

## Slide 27
Notes: Supplementary Figure 25. Evolution of the absorbance spectra of unencapsulated FA0.83Cs0.17Pb(I0.6Br0.4)3 films with or without 15 mol% MACl additives stored at dark, ambient conditions (25 °C, 40% RH in air) for 17 days. Two samples were aged and measured for each variable.

## Slide 28
Notes: Supplementary Figure 26. Quasi-Fermi level splitting (QFLS) maps taken using an in house-built photoluminescence measurement setup on (a) thin films on glass (b) full devices of perovskite with 15 mol% MACl additive and (c) thin films on glass (d) full devices of control perovskite compositions. Me-4PACz and C60 were used as HTL and ETL respectively in the full devices. Two films and two pixels were measured for each variable, small variations in the absolute QFLS values between different samples are shown in the graph.

## Slide 29
(c)
(d)
(a)
(b)
Notes: Supplementary Figure 27. Long-term photo and thermal stability measurements of control or 15 mol% MACl additive PSCs based on PTAA or Me-4PACz: (a) ηmpp, (b) steady-state VOC, (c) steady-state JSC and (d) quasi-FF. All the devices were encapsulated and aged under 1-sun illumination, at open-circuit condition, 65 °C in ambient air (~ 40% RH) over 300 hours. Medians and standard median deviations of 40 devices (10 devices for each variable) are shown in the graph.

## Slide 30
(a)
(c)
(b)
(d)
Notes: Supplementary Figure 28. (a) ηmpp, (b) steady-state VOC, (c) steady-state JSC and (d) quasi-FF of FA0.75Cs0.25Pb(I0.7Br0.3) with 10 mol% excess of MAPbCl3 triple halide perovskite solar cells employing PTAA, Poly-TPD and Me-4PACz respectively as hole transport layers. These devices were fabricated within one batch of experiment. Any pixel with ηmpp ≤ 75% ηmpp of the champion device are cut off from the figure.

## Slide 31
Notes: Supplementary Figure 29. J-V scan of the champion device based on FA0.75Cs0.25Pb(I0.7Br0.3) with 10 mol% excess of MAPbCl3 triple halide perovskite solar cells with Me-4PACz as HTL.